## Slide 1: Improving 3D NAND Flash Memory Lifetime by Tolerating Early Retention Loss and Process Variation
Yixin Luo Saugata Ghose Yu Cai Erich F. Haratsch Onur Mutlu
Notes: Thank you for the introduction. Today, I will present our work about …

## Slide 2: NAND Flash Memory Lifetime Problem
Wearout (Program/Erase Cycles, or PEC)
Raw Bit Error Rate (RBER)
Gen N
ECC Limit
Lifetime
ECC Limit
Lifetime
Gen N+1
Flash lifetime decreases in each generation despite increased ECC strength
Notes: NAND flash memory is a type of storage media widely used in today’s SSDs.
NAND flash memory wears out as we write more data to it.
This means that the raw bit error rate (on the y-axis) increases as the program/erase cycle (on the x-axis) increases, as we show on this figure.
These errors are tolerated by ECC code, which can correct raw bit errors up to a certain limit. When RBER goes beyond this limit, flash lifetime end.
In each new generation, we trade off reliability for higher storage density. So flash lifetime decreases despite the increased ECC strength and ECC limit.

## Slide 3: Planar vs. 3D NAND Flash Memory
Planar NAND Flash Memory
3D NAND Flash Memory
Scaling
Reliability
Reduce flash cell size,
Reduce distance b/w cells
Increase # of layers
Scaling hurts reliability
Not well studied!
Notes: To further increase storage density, manufacturers developed 3D NAND technology, which stacks dozens of layers of flash memory on top of each other.
This new technology changes a lot of designs inside flash memory, from circuit-level design to flash cell organization.
But at this point, due to its recent development, the implication of 3D NAND technology on flash reliability is not well studied.

## Slide 4: Executive Summary
Problem: 3D NAND error characteristics are not well studied
Goal: Understand & mitigate 3D NAND errors to improve lifetime
Contribution 1: Characterize real 3D NAND flash chips
  Process variation: 21× error rate difference across layers
  Early retention loss: Error rate increases by 10× after 3 hours
  Retention interference: Not observed before in planar NAND
Contribution 2: Model RBER and threshold voltage
  RBER (raw bit error rate) variation model
  Retention loss model
Contribution 3: Mitigate 3D NAND flash errors
  LaVAR: Layer Variation Aware Reading
  LI-RAID: Layer-Interleaved RAID
  ReMAR: Retention Model Aware Reading
  Improve flash lifetime by 1.85× or reduce ECC overhead by 78.9%
Notes: In this work, our goal is to …
In the xth contribution, we …

## Slide 5: Agenda
Background & Introduction
Contribution 1: Characterize real 3D NAND flash chips
Contribution 2: Model RBER and threshold voltage
Contribution 3: Mitigate 3D NAND flash errors
Conclusion

## Slide 6: Agenda
Background & Introduction
Contribution 1: Characterize real 3D NAND flash chips
  Process variation
  Early retention loss
  Retention interference
Contribution 2: Model RBER and threshold voltage
Contribution 3: Mitigate 3D NAND flash errors
Conclusion

## Slide 7: Process Variation Across Layers
Layer M
Layer 1
Layer 0
…
…
…
…
…
…
…
BL N
BL 1
BL 0
…
…
…
…
Flash Cell
Flash cells on different layers may have different error characteristics
Notes: This figure shows how flash cells are organized in a 3-dimensional manner, with M+1 layers.
Each layer of a vertical bitline is a flash cell.
The key takeaway is the flash cells on different layers may have different error characteristics, because of the systematic process variation caused by the way how these vertical bitlines are manufactured.
So our goal is to experimentally characterize this phenomenon using real chips.

## Slide 8: Characterization Methodology
Modified firmware version in the flash controller
  Controls the read reference voltage of the flash chip
  Bypasses ECC to get raw data (with raw bit errors)
Analysis and post-processing of the data on the server
SSD
Server
Notes: Here is the methodology we use.
Our characterization platform consists of a form-factor SSD connected to a server machine.
We use a modified firmware version in the flash controller, which allows us to control the read reference voltage of the flash chip,
and to bypass error correction to get raw NAND data.

## Slide 9: Layer-to-Layer Process Variation
21×
2.4×
Max RBER
Notes: Here is the characterization result. X-axis shows …, y-axis shows …
We make several observations from the data.
Large variation in RBER across different layers, this phenomenon is called layer-to-layer
RBER variation caused by LSB-MSB page, we call this LSB-MSB RBER variation
Max RBER in middle layers
Consistent across chips

## Slide 10: Layer-to-Layer Process Variation
Large RBER variation across layers and LSB-MSB pages
Notes: Here is the characterization result. X-axis shows …, y-axis shows …
We make several observations from the data.
Large variation in RBER caused by layers
RBER variation caused by LSB-MSB page
Max RBER in middle layers
Consistent across chips
The key takeaway is that due to layer-to-layer process variation, there are large RBER variations.

## Slide 11: Retention Loss Phenomenon
Most dominant type of error in planar NAND. Is this true for 3D NAND as well?
Control Gate
Substrate
Drain
Source
Planar NAND Cell
Floating Gate (Conductor)
Gate Oxide
3D NAND Cell
Substrate
Source
Drain
Charge Trap
(Insulator)
Control Gate
Gate Oxide
Tunnel Oxide
Tunnel Oxide
Notes: The second phenomenon we characterize is retention loss.
NAND flash cell stores data in the form of electric charges.
Retention loss refers to the phenomenon that charge leaks away over time, leading to retention errors.
Prior work has shown that retention error is the most dominant type of error in planar NAND flash memory.
So how about 3D NAND, which uses a new cell design?
Will this change the behavior of retention loss? That’s what we are about to find out.

## Slide 12: Early Retention Loss
10x
3 hours
10x
11 days
3 years
10x
Retention errors increase quickly immediately after programming
Notes: Here is the characterization result. X-axis shows …, y-axis shows … blue curve … orange curve ….
We make several observations from the data.
1. Retention errors increase much faster in 3D NAND than planar NAND
2. Retention errors increase quickly immediately after programming

## Slide 13: Characterization Summary
Layer-to-layer process variation
  Large RBER variation across layers and LSB-MSB pages
   Need new mechanisms to tolerate RBER variation!
Early retention loss
  RBER increases quickly after programming
   Need new mechanisms to tolerate retention errors!
Retention interference
  Amount of retention loss correlated with neighbor cells’ states
   Need new mechanisms to tolerate retention interference!
More threshold voltage and RBER results in the paper: 3D NAND P/E cycling, program interference, read disturb, read variation, bitline-to-bitline process variation
Our approach based on insights developed via our experimental characterization: Develop error models, and build online error mitigation mechanisms using the models
Notes: As a summary, we have discussed layer-to-layer process variation and early retention loss. Both are new and different in 3D NAND.
In our paper, we also show retention interference phenomenon where the amount of …, which is also new in 3D NAND.
So these three new phenomena in 3D NAND motivate us to design new mechanisms to tolerate 3D NAND errors.
We have many other results regarding threshold voltage and RBER, which we don’t have time to talk about.
Next, we will discuss our approach to model and mitigate these new 3D NAND errors characteristics.

## Slide 14: Agenda
Background & Introduction
Contribution 1: Characterize real 3D NAND flash chips
Contribution 2: Model RBER and threshold voltage
  Retention loss model
  RBER variation model
Contribution 3: Mitigate 3D NAND flash errors
Conclusion

## Slide 15: What Do We Model?
11
01
00
10
MSB
LSB
Va
Vb
Vc
Read Reference Voltages
Probability
Threshold Voltage (Vth)
Threshold Voltage Distribution
Raw Bit Errors
Notes: First, let’s look at what are the things that we modeled.
NAND flash memory stores data as the threshold voltage of a flash cell.
The flash chips that we study in this work utilizes the multi-level cell technology, which divides the threshold voltage range into 4 possible states, so that each cell can store a 2-bit value, consisting of MSB and LSB.
We model the threshold voltage distribution of each state as a Gaussian distribution, with mean and variance.
The bit values stored in flash memory can be read by applying three read reference voltages at the boundary of the 4 states, Va Vb and Vc.
The cells in each distribution that goes across these reference voltages will cause raw bit errors, which changes over time.

## Slide 16: Optimal Read Reference Voltage
Va
Vb
Vc
Probability
Threshold Voltage (Vth)
Raw Bit Errors
Notes: Raw bit errors are decided by two things.
First is the distribution shifts quickly due to retention loss. If we keep the read reference voltage same, raw bit errors will increase.
Read reference voltage also affects raw bit errors. If we shift the read reference voltage accordingly, we can minimize raw bit errors.
We call this the optimal read reference voltage. Our goal is to model the shift accurately to reduce raw bit errors.

## Slide 17: Retention Loss Model
Early retention loss can be modeled as
a simple linear function of log(retention time)
Notes: This figure shows a part of our retention model. X-axis shows …, y-axis shows the optimal read reference voltage, each subfigure shows Va Vb Vc respectively
Blue dots are the actual optimal read reference voltages from measured data.
We find that the voltage shift due to retention loss fits a linear trend of the logarithm of retention time.
In fact, we find that other parameters also follows a linear function.

## Slide 18: Retention Loss Model
Goal: Develop a simple linear model that can be used online
Models
  Optimal read reference voltage (Vb and )
  Raw bit error rate ()
  Mean and standard deviation of threshold voltage distribution ( and )
As a function of
  Retention time ()
  P/E cycle count
e.g.,
Model error <1 step for Vb and
Adjusted R2 > 89%
Notes: Here is an overview of our full model. We refer to our paper for more detailed information.
Our retention loss model predicts …
And it models these variables as a function of …
Here is an example of how simple our model is to predict the optimal read reference voltage
Our model is highly accurate, …

## Slide 19: RBER Variation Model
Variation-agnostic Vopt
Same Vref for all layers optimized for the entire block
Variation-aware Vopt
Different Vref optimized for each layer
KL-divergence error = 0.09
RBER distribution follows gamma distribution
Notes: This figure shows the distribution of per-page RBER within a flash block. X-axis shows …, y-axis shows …. The bars show the actual RBER distribution.
We find that this variation can be accurately modeled by a gamma distribution, regardless of which read reference voltage is used.
Variation-aware Vopt improves both average and worst-case RBER
RBER distribution follows gamma distribution: KL-divergence error = 0.09
Large gap between worst-case RBER and average RBER  Need new mechanisms to narrow the RBER distribution!

## Slide 20: Agenda
Background & Introduction
Contribution 1: Characterize real 3D NAND flash chips
Contribution 2: Model RBER and threshold voltage
Contribution 3: Mitigate 3D NAND flash errors
  LaVAR: Layer Variation Aware Reading
  LI-RAID: Layer-Interleaved RAID
  ReMAR: Retention Model Aware Reading
Conclusion

## Slide 21: LaVAR: Layer Variation Aware Reading
Layer-to-layer process variation
  Error characteristics are different in each layer
Goal: Adjust read reference voltage for each layer
Key Idea: Learn a voltage offset (Offset) for each layer
Mechanism
  Offset: Learned once for each chip & stored in a table
    Uses Bytes memory per chip
  : Predicted by any existing Vopt model
    E.g., ReMAR [Luo+Sigmetrics’18], HeatWatch [Luo+HPCA’18], OFCM [Luo+JSAC’16], ARVT [Papandreou+GLSVLSI’14]
Reduces RBER on average by 43% (based on our characterization data)

## Slide 22: LI-RAID: Layer-Interleaved RAID
Layer-to-layer process variation
  Worst-case RBER much higher than average RBER
Goal: Significantly reduce worst-case RBER
Key Idea
  Group flash pages on less reliable layers with pages on more reliable layers
  Group MSB pages with LSB pages
Mechanism
  Reorganize RAID layout to eliminate worst-case RBER
  <0.4% storage overhead

## Slide 23: Conventional RAID
Wordline # | Layer # | Page | Chip 0 | Chip 1 | Chip 2 | Chip 3
0 | 0 | MSB | Group 0 | Group 0 | Group 0 | Group 0
0 | 0 | LSB | Group 1 | Group 1 | Group 1 | Group 1
1 | 1 | MSB | Group 2 | Group 2 | Group 2 | Group 2
1 | 1 | LSB | Group 3 | Group 3 | Group 3 | Group 3
2 | 2 | MSB | Group 4 | Group 4 | Group 4 | Group 4
2 | 2 | LSB | Group 5 | Group 5 | Group 5 | Group 5
3 | 3 | MSB | Group 6 | Group 6 | Group 6 | Group 6
3 | 3 | LSB | Group 7 | Group 7 | Group 7 | Group 7
Worst-case RBER in any layer limits the lifetime of conventional RAID

## Slide 24: LI-RAID: Layer-Interleaved RAID
Wordline # | Layer # | Page | Chip 0 | Chip 1 | Chip 2 | Chip 3
0 | 0 | MSB | Group 0 | Blank | Group 4 | Group 3
0 | 0 | LSB | Group 1 | Blank | Group 5 | Group 2
1 | 1 | MSB | Group 2 | Group 1 | Blank | Group 5
1 | 1 | LSB | Group 3 | Group 0 | Blank | Group 4
2 | 2 | MSB | Group 4 | Group 3 | Group 0 | Blank
2 | 2 | LSB | Group 5 | Group 2 | Group 1 | Blank
3 | 3 | MSB | Blank | Group 5 | Group 2 | Group 1
3 | 3 | LSB | Blank | Group 4 | Group 3 | Group 0
Any page with worst-case RBER can be corrected by other reliable pages in the RAID group

## Slide 25: LI-RAID: Layer-Interleaved RAID
Layer-to-layer process variation
  Worst-case RBER much higher than average RBER
Goal: Significantly reduce worst-case RBER
Key Idea
  Group flash pages on less reliable layers with pages on more reliable layers
  Group MSB pages with LSB pages
Mechanism
  Reorganize RAID layout to eliminate worst-case RBER
  <0.8% storage overhead
Reduces worst-case RBER by 66.9% (based on our characterization data)

## Slide 26: ReMAR: Retention Model Aware Reading
Early retention loss
  Threshold voltage shifts quickly after programming
Goal: Adjust read reference voltages based on retention loss
Key Idea: Learn and use a retention loss model online
Mechanism
  Periodically characterize and learn retention loss model online
  Retention time = Read timestamp - Write timestamp
    Uses 800 KB memory to store program time of each block
  Predict retention-aware Vopt using the model
Reduces RBER on average by 51.9% (based on our characterization data)

## Slide 27: Impact on System Reliability
Chart: P/E Cycle Count
| 0 | 1000 | 2000 | 3000 | 4000 | 5000 | 6000 | 7000 | 8000 | 9000 | 10000 | 12000 | 14000 | 16000 | 17564.4126598027 | 17569.484198944101 | 21419.902354252001 | 24595.6098362782
Baseline | 0.00028064 | 0.00033928 | 0.00042305 | 0.00069531 | 0.00066599 | 0.00063667 | 0.00090892 | 0.00088798 | 0.0011686 | 0.0010932 | 0.0018681 | 0.004197 | 0.0093824 | 0.012624
State-of-the-art | 0.00012566 | 0.00015079 | 0.0001466 | 0.0002555 | 0.00017592 | 0.00018011 | 0.00023456 | 0.00025969 | 0.00028901 | 0.00041886 | 0.00065342 | 0.0016796 | 0.0041467 | 0.0056881 | 0.01
LaVAR | 0.00012147 | 0.00013822 | 0.00016335 | 0.00018011 | 0.00013822 | 0.00015917 | 0.00016335 | 0.00021362 | 0.00024713 | 0.00037697 | 0.00056965 | 0.0013194 | 0.0031791 | 0.0055206 | 0.0099808 | 0.01
LaVAR + LI-RAID | 2.7226e-05 | 3.2723e-05 | 3.7697e-05 | 4.6074e-05 | 4.5027e-05 | 4.9216e-05 | 5.864e-05 | 7.4086e-05 | 9.372e-05 | 0.00011519 | 0.00016571 | 0.00033509 | 0.00078562 | 0.0014286 | 0.0025051 | 0.0025097 | 0.01
This Work | 2.2549e-05 | 1.9401e-05 | 1.9202e-05 | 2.0912e-05 | 2.0212e-05 | 1.892e-05 | 2.2975e-05 | 2.7504e-05 | 3.3715e-05 | 3.4839e-05 | 5.2988e-05 | 0.00010715 | 0.00025121 | 0.0004568 | 0.00080105 | 0.00080251 | 0.0031976 | 0.01
ECC Limit
85% longer flash lifetime
79% lower ECC storage overhead
LaVAR, LI-RAID, and ReMAR improve flash lifetime or reduce ECC overhead significantly

## Slide 28: Error Mitigation Techniques Summary
LaVAR: Layer Variation Aware Reading
  Learn a Vopt offset for each layer and apply layer-aware Vopt
LI-RAID: Layer-Interleaved RAID
  Group flash pages on less reliable layers with pages on more reliable layers
  Group MSB pages with LSB pages
ReMAR: Retention Model Aware Reading
  Learn retention loss model and apply retention-aware Vopt
Benefits:
Improve flash lifetime by 1.85× or reduce ECC overhead by 78.9%
ReNAC (in paper): Reread a failed page using Vopt based on the retention interference induced by neighbor cell

## Slide 29: Agenda
Background & Introduction
Contribution 1: Characterize real 3D NAND flash chips
Contribution 2: Model RBER and threshold voltage
Contribution 3: Mitigate 3D NAND flash errors
Conclusion

## Slide 30: Conclusion
Problem: 3D NAND error characteristics are not well studied
Goal: Understand & mitigate 3D NAND errors to improve lifetime
Contribution 1: Characterize real 3D NAND flash chips
  Process variation: 21× error rate difference across layers
  Early retention loss: Error rate increases by 10× after 3 hours
  Retention interference: Not observed before in planar NAND
Contribution 2: Model RBER and threshold voltage
  RBER (raw bit error rate) variation model
  Retention loss model
Contribution 3: Mitigate 3D NAND flash errors
  LaVAR: Layer Variation Aware Reading
  LI-RAID: Layer-Interleaved RAID
  ReMAR: Retention Model Aware Reading
  Improve flash lifetime by 1.85× or reduce ECC overhead by 78.9%
Notes: In this work, our goal is to …
In the xth contribution, we …

## Slide 31: Improving 3D NAND Flash Memory Lifetime by Tolerating Early Retention Loss and Process Variation
Yixin Luo Saugata Ghose Yu Cai Erich F. Haratsch Onur Mutlu
Notes: Thank you for the introduction. Today, I will present our work about …

## Slide 32: Backup Slides

## Slide 33: LI-RAID: Layer-Interleaved RAID
Wordline # | Layer # | Page | Chip 0 | Chip 1 | Chip 2 | Chip 3
0 | 0 | MSB | Group 0 | (Group 6) | Group 4 | Group 3
0 | 0 | LSB | Group 1 | (Group 7) | Group 5 | Group 2
1 | 1 | MSB | Group 2 | Group 1 | Blank | Group 5
1 | 1 | LSB | Group 3 | Group 0 | Blank | Group 4
2 | 2 | MSB | Group 4 | Group 3 | Group 0 | Blank
2 | 2 | LSB | Group 5 | Group 2 | Group 1 | Blank
3 | 3 | MSB | Blank | Group 5 | Group 2 | Group 1
3 | 3 | LSB | Blank | Group 4 | Group 3 | Group 0
Violating program sequence (in-order from top to bottom)
Groups 0&1 vulnerable to program interference by Groups 2&3

## Slide 34: How Does NAND Flash Memory Work?
NAND Flash Memory
Flash Cell
Higher Voltage State
Lower Voltage State
Data Value = 0
Data Value = 1
–
–
–
Read Reference Voltage
Charge = Threshold Voltage
Notes: 3D NAND flash memory consists of flash cells, each of which holds different amount of charge which determines the threshold voltage of the cell.
And the threshold voltage determines the data value stored in that cell.
For example, for a cell that stores one bit of data, 0 can be assigned to higher voltage state, and 1 assigned to lower voltage state.
We can sense the data value by applying a read reference voltage to the cell that can distinguish between these two states.

## Slide 35: MLC Threshold Voltage Distribution
11
01
00
10
Probability
Threshold Voltage
–
–
–
Highest Voltage State
Lowest Voltage State
–
–
–
LSB Read Reference Voltage
MSB Read Reference Voltage
MSB Read Reference Voltage
Threshold Voltage Distribution
MSB
LSB
Notes: Each MLC cell has 4 threshold voltage states. We assign a different 2-bit value to each state..
And they are read by three read reference voltages instead of one.
To better understand the reliability of the cell, we typically model the probability distribution (point) of the threshold voltage (point) of each state as a probability density function. We call this the threshold voltage distribution.

## Slide 36: 3D NAND Flash Cell
Control Gate
Substrate
Drain
Source
Floating Gate Cell
Floating Gate (Conductor)
Gate Oxide
3D Charge Trap Cell
Substrate
Source
Drain
Charge Trap
(Insulator)
Control Gate
Gate Oxide
Tunnel Oxide
Tunnel Oxide
Notes: The 3D NAND chips that we studied use 3D charge-trap cell, and here is how it compares with a floating gate cell used in planar NAND.

## Slide 37: 3D NAND Organization
Block K+2
Block K+1
Block K
Layer M
Layer 1
Layer 0
Wordline 0
…
…
…
…
…
…
…
Wordline 1
BL N
BL 1
BL 0
Wordline M
…
…
…
…

## Slide 38: MLC NAND Page Organization
Block K+2
Block K+1
Block K
Layer M
Layer 1
Layer 0
Wordline 0
…
…
…
…
…
…
…
Wordline 1
BL N
BL 1
BL 0
Wordline M
…
…
…
…
MSB page
LSB page
MSB page
LSB page
MSB page
LSB page

## Slide 39: Root Cause of Early Retention Loss
Control Gate
Substrate
Drain
Source
Floating Gate Cell
Floating Gate (Conductor)
Gate Oxide
3D Charge Trap Cell
Substrate
Source
Drain
Charge Trap
(Insulator)
Control Gate
Gate Oxide
Tunnel Oxide
Tunnel Oxide
Oxide layers are designed to be thinner in 3D NAND [Samsung WhitePaper’14]  Charges near the surface of charge trap layer leaks faster
Notes: The 3D NAND chips that we studied use 3D charge-trap cell, and here is how it compares with a floating gate cell used in planar NAND.

## Slide 40: Retention Interference
Chart: # of Voltage Steps Shifted Over 24-Day Retention
| V=01 | V=00 | V=10
N=11 | 6.3339 | 11.375 | 17.9608
N=01 | 5.7392 | 10.6764 | 17.1886
N=00 | 5.4329 | 10.451 | 17.0238
N=10 | 5.2402 | 10.3922 | 16.9554
Neighbor
Neighbor
Victim
V: Victim
N: Neighbor
< 2
steps
Retention loss speed correlated with neighbor cells’ state
Notes: The retention loss speed of a victim cell depends on the threshold voltage of its directly-connect neighboring cell
  Retention interference is small in current generation 3D NAND, but it will increase in future generations as layer numbers increase and distance between layers decrease  Need new mechanisms!

## Slide 41: Retention Loss Model
Because of early retention loss, Vopt shifts quickly after programming
Linear correlation between Vopt and log(t : retention time)
Linear correlation between log(RBER) and log(t)  Develop a simple linear model that can be used online

## Slide 42: Error Mitigation Techniques
LaVAR: Layer Variation Aware Reading
  Learn a Vopt offset for each layer and apply variation-aware Vopt
  Reduces RBER on average by 43%
  Uses Byte memory per chip
LI-RAID: Layer-Interleaved RAID
  Group flash pages on less reliable layers with pages on more reliable layers
  Group MSB pages with LSB pages
  Reduce worst-case RBER by 66.9%
  <0.4% storage overhead
ReMAR: Retention Model Aware Reading
  Learn retention loss model and apply retention-aware Vopt
  Reduce RBER on average by 51.9%
  Uses 800 KB memory to store program time of each block

## Slide 43: LI-RAID Data Layout
Page/Wordline #/Layer # | Chip 0 | Chip 1 | Chip 2 | Chip 3
MSB/Wordline 0/Layer 0 | Group 0 | Blank | Group 4 | Group 3
LSB/Wordline 0/Layer 0 | Group 1 | Blank | Group 5 | Group 2
MSB/Wordline 1/Layer 1 | Group 2 | Group 1 | Blank | Group 5
LSB/Wordline 1/Layer 1 | Group 3 | Group 0 | Blank | Group 4
MSB/Wordline 2/Layer 2 | Group 4 | Group 3 | Group 0 | Blank
LSB/Wordline 2/Layer 2 | Group 5 | Group 2 | Group 1 | Blank
MSB/Wordline 3/Layer 3 | Blank | Group 5 | Group 2 | Group 1
LSB/Wordline 3/Layer 3 | Blank | Group 4 | Group 3 | Group 0

## Slide 44: Threshold Voltage Shift

## Slide 45: No Programming Errors

## Slide 46: P/E Cycling Effect on Threshold Voltage

## Slide 47: P/E Cycling Errors

## Slide 48: P/E Cycling Effect on Optimal Read Reference Voltages

## Slide 49: Program Interference Effect & Interference Correlation
Block K+1
Block K
Victim
2.7%
.057%
.080%
-.040%
.014%
-.040%
.014%
BL M
BL M-1
BL M+1
WL N
WL N-1
WL N+1
WL N+2
y
z
x
Next bitline
Next wordline+bitline
Previous wordline
Next wordline

## Slide 50: Program Interference vs. PEC

## Slide 51: Early Retention Loss Effect on Threshold Voltage

## Slide 52: Early Retention Loss Errors

## Slide 53: Early Retention Loss Effect on Optimal Read Reference Voltages

## Slide 54: Read Disturb Effect on Threshold Voltage

## Slide 55: Read Disturb Errors

## Slide 56: Read Variation Errors

## Slide 57: Read Variation Errors vs. RBER

## Slide 58: Read Disturb Effect on Optimal Read Reference Voltages

## Slide 59: RBER Breakdown