## Slide 1: Revisiting RowHammer An Experimental Analysis of Modern Devices and Mitigation Techniques
Jeremie S. Kim Minesh Patel
A. Giray Yağlıkçı Hasan Hassan
Roknoddin Azizi Lois Orosa Onur Mutlu
Notes: Hello, my name is Jeremie Kim and I will be presenting our work revisiting rowhammer: an experimental analysis of modern devices and mitigation techniques

## Slide 2: Executive Summary
Motivation: Denser DRAM chips are more vulnerable to RowHammer but no characterization-based study demonstrates how vulnerability scales
Problem: Unclear if existing mitigation mechanisms will remain viable for future DRAM chips that are likely to be more vulnerable to RowHammer
Goal:
  Experimentally demonstrate how vulnerable modern DRAM chips are to RowHammer and study how this vulnerability will scale going forward
  Study viability of existing mitigation mechanisms on more vulnerable chips
Experimental Study: First rigorous RowHammer characterization study across a broad range of DRAM chips
  1580 chips of different DRAM {types, technology node generations, manufacturers}
  We find that RowHammer vulnerability worsens in newer chips
RowHammer Mitigation Mechanism Study: How five state-of-the-art mechanisms are affected by worsening RowHammer vulnerability
  Reasonable performance loss (8% on average) on modern DRAM chips
  Scale poorly to more vulnerable DRAM chips (e.g., 80% performance loss)
Conclusion: it is critical to research more effective solutions to RowHammer for future DRAM chips that will likely be even more vulnerable to RowHammer
Notes: I will first begin with an executive summary
[CLICK] Denser DRAM chips are more vulnerable to RowHammer but there is no characterization-based study that demonstrates how exactly the vulnerability scales
[CLICK] The problem is that it is unclear whether current mitigation mechanisms will remain viable for future DRAM chips that are likely to be more vulnerable to RowHammer
[CLICK] The goal of this work is to [CLICK] first experimentally demonstrate how vulnerable modern DRAM chips are to RowHammer and study how this vulnerability will scale going forward
[CLICK] Secondly, we want to study the viability of current mitigation mechanisms on more vulnerable chips
[CLICK] We are the first experimental study to present a rigorous RowHammer failure characterization study across a broad range of DRAM chips
[CLICK] We characterize 1580 DRAM chips across different DRAM types and technology node generations, across the three major DRAM manufacturers
[CLICK] And we demonstrate that the RowHammer vulnerability worsens in newer chips
[CLICK] We also study RowHammer mitigation mechanisms in simulation and show how 5 state-of-the-art mechanisms are affected by a worsening RowHammer vulnerability
[CLICK] We find that these mitigation mechanisms have reasonable performance loss on modern DRAM chips, but [CLICK] scale poorly to more vulnerable DRAM chips
[CLICK] We conclude that it is critical to research more effective solutions to RowHammer for future DRAM chips that will likely be even more vulnerable to RowHammer
=============
reduce text on this slide.

## Slide 3: Outline
RowHammer Introduction
DRAM Background
Motivation and Goal
Experimental Methodology
Characterization Results
Evaluation of Mitigation Mechanisms
RowHammer Solutions Going Forward
Conclusion
Notes: Here is the outline for the talk today

## Slide 4: Outline
RowHammer Introduction
DRAM Background
Motivation and Goal
Experimental Methodology
Characterization Results
Evaluation of Mitigation Mechanisms
RowHammer Solutions Going Forward
Conclusion
Notes: I will begin with a brief introduction of the RowHammer phenomenon

## Slide 5: The RowHammer Vulnerability
Row 0
Row 1
Row 2
Row 3
Row 4
Repeatedly opening (activating) and closing (precharging)
a DRAM row causes RowHammer bit flips in nearby cells
Row 2
open
Row 1
Row 3
Row 2
closed
Row 2
open
Row 1
Row 3
Row 0
Row 4
Row 2
closed
Victim Row
Victim Row
Victim Row
Victim Row
Aggressor Row
Row 2
open
Row 2
closed
Aggressor Row
DRAM Chip
Notes: In order to access data from a DRAM row, say row 2, the memory controller must first open or activate the row [CLICK].
After all requests are serviced from row 2, the memory controller must close or precharge the row [CLICK] in order to begin accessing data from another row.
[BACK & FORTH] Due to an increase in cell-to-cell interference as a likely result of increased cell packing density, rapidly activating and precharging a DRAM row can result in bit flips in nearby rows [CLICK]
[FORTH & BACK] Continuing to access the same row results in even more failures in nearby rows. This phenomenon is known as RowHammer. [CLICK]
We refer to the rapidly accessed row as an aggressor row and the rows containing bit flips as victim rows.
========
more polish text too close made better. More col;orful. Better figure too.

## Slide 6: Outline
RowHammer Introduction
DRAM Background
Motivation and Goal
Experimental Methodology
Characterization Results
Evaluation of Mitigation Mechanisms
RowHammer Solutions Going Forward
Conclusion
Notes: I will now discuss the DRAM background in the context of RowHammer bit flips and how they occur

## Slide 7: DRAM Organization
DRAM Bank
Row of storage cells
Row 1
Row 2
Row 3
Row 4
Notes: DRAM is comprised of an array of cells that store data as charge, and are organized into rows

## Slide 8: DRAM Cell Leakage
Each cell encodes information in leaky capacitors
wordline
capacitor
access
transistor
bitline
Stored data is corrupted if too much charge leaks (i.e., the capacitor voltage degrades too much)
charge
leakage
paths
[Patel+, ISCA’17]
Notes: Each cell encodes data in fundamentally leaky capacitors [CLICK] Here is a simplified diagram of a DRAM cell, where the capacitor in red stores the data and the access transistor gates access to the data
[CLICK]
There are a number of leakage paths by which charge can enter or exit the capacitor.
[CLICK]
The important thing to note is that stored data can be corrupted if too much charge leaks
Which is the same as saying if the capacitor voltage degrades too much
[END]

## Slide 9: DRAM Refresh
Periodic refresh operations preserve stored data
Capacitor voltage (Vdd)
100%
0%
Vmin
Refresh Window
Refresh Operations
time
REF
REF
REF
Notes: Here, we have a simplified diagram of the capacitor voltage over time
We see that the voltage decreases over time in an exponential decay.
There’s a threshold Vmin under which we can no longer guarantee that we will correctly read the data that was originally stored in the cell.
[CLICK]
As long as a cell’s voltage remains above this line, we consider this a retention success.
[CLICK]
However, as soon as the voltage drops below Vmin, we consider this a retention failure
In order to prevent failures from charge leakage known as retention failures, [CLICK] periodic refresh operations are issued to recharge the capacitor voltage. [CLICK] The interval between refresh commands are referred to as the refresh window.

## Slide 10: RowHammer Bit Flips
Capacitor voltage (Vdd)
100%
0%
Vmin
time
REF
REF
REF
RowHammer Attack:
Accesses to nearby row
RowHammer
Bit Flip
Notes: Now lets take a look at this diagram in the context of a RowHammer attack.
[CLICK] If enough activations are issued to a nearby row within a refresh window, the charge leakage rate can be accelerated to the point of failure.
Subsequent refresh commands now see this bit as a 0 value and maintain the discharged state of the cell

## Slide 11: Cell-to-Cell Variation
Capacitor voltage (Vdd)
100%
0%
Vmin
time
REF
REF
REF
Different RowHammer vulnerabilities
Some cells are more vulnerable due to process variation
RowHammer Attack:
Accesses to nearby row
Notes: We note that due to manufacturing variation in DRAM circuit elements, [CLICK] different cells are affected by RowHammer at varying degrees. We see that we are able to Induce a RowHammer bit flip in the cells represented by the black and blue curves but not the green curve
=======

## Slide 12: Outline
RowHammer Introduction
DRAM Background
Motivation and Goal
Experimental Methodology
Characterization Results
Evaluation of Mitigation Mechanisms
RowHammer Solutions Going Forward
Conclusion
Notes: I will now discuss the motivation and the goal of our work

## Slide 13: Motivation
  Denser DRAM chips are more vulnerable to RowHammer
  Three prior works [Kim+, ISCA’14], [Park+, MR’16], [Park+, MR’16], over the last six years provide RowHammer characterization data on real DRAM
  However, there is no comprehensive experimental study that demonstrates how vulnerability scales across DRAM types and technology node generations
  It is unclear whether current mitigation mechanisms will remain viable for future DRAM chips that are likely to be more vulnerable to RowHammer
Notes: The motivation for this study is that
[CLICK] denser DRAM chips are more vulnerable to RowHammer
[CLICK] Three prior works provide RowHammer characterization data on real DRAM chips.
[CLICK] However, there is no comprehensive experimental study that demonstrates how the RowHammer vulnerability scales across DRAM types and technology node generations and as DRAM chips become more dense
[CLICK] Therefore it is hard to identify whether current mitigation mechanisms will remain viable for future DRAM chips that are likely to be more vulnerable to RowHammer

## Slide 14: Goal
  Experimentally demonstrate how vulnerable modern DRAM chips are to RowHammer and predict how this vulnerability will scale going forward
  Examine the viability of current mitigation mechanisms on more vulnerable chips
Notes: The goal of this work is to
[CLICK] First, experimentally demonstrate how vulnerable modern DRAM chips are to RowHammer and predict how this vulnerability will scale going forward and
[CLICK] Second, we want to study the viability of current mitigation mechanisms on more vulnerable chips.

## Slide 15: Outline
RowHammer Introduction
DRAM Background
Motivation and Goal
Experimental Methodology
Characterization Results
Evaluation of Mitigation Mechanisms
RowHammer Solutions Going Forward
Conclusion
Notes: I will now present our experimental methodology for DRAM characterization

## Slide 16: DRAM Testing Infrastructures
Three separate testing infrastructures
  DDR3: FPGA-based SoftMC [Hassan+, HPCA’17]
    (Xilinx ML605)
  DDR4: FPGA-based SoftMC [Hassan+, HPCA’17]
    (Xilinx Virtex UltraScale 95)
  LPDDR4: In-house testing hardware for LPDDR4 chips
All provide fine-grained control over DRAM commands, timing parameters and temperature
DDR4 DRAM testing infrastructure
Notes: We use three separate testing infrastructures for each DRAM standard or type that we characterize in this work.
We use one FPGA-based SoftMC infrastructure for DDR3 chips and another for DDR4 chips.
We also use an in-house testing hardware infrastructure to examine LPDDR4 chips
Across our infrastructures, we have fine-grained control over DRAM commands, timing parameters, and temperatures
Below is an example of our FPGA-based DDR4 testing infrastructure.
=======

## Slide 17: DRAM Chips Tested
1580 total DRAM chips tested from 300 DRAM modules
Three major DRAM manufacturers {A, B, C}
Three DRAM types or standards {DDR3, DDR4, LPDDR4}
  LPDDR4 chips we test implement on-die ECC
Two technology nodes per DRAM type {old/new, 1x/1y}
  Categorized based on manufacturing date, datasheet publication date, purchase date, and characterization results
Type-node: configuration describing a chip’s type and technology node generation: DDR3-old/new, DDR4-old/new, LPDDR4-1x/1y
Notes: Here we show a table that lists all the DRAM chips that we test
[CLICK] We characterize over 1500 DRAM chips from 300 DRAM modules
[CLICK] spanning the three major DRAM manufacturers which we anonymize as A, B, and C
[CLICK] of three DRAM types or standards DDR3, DDR4, and LPDDR4. We note that LPDDR4 chips that we test implement on-die ECC.
[CLICK] We identify two technology nodes per DRAM type (old/new, 1x and 1y) , which we categorize based on manufacturing date, datasheet publication date, purchase date, and characterization results
[CLICK] we define the term type-node which refers to the configuration describing a chip’s type and technology node generation. Across the chips we characterize, we identify the 6 DRAM type-node configurations listed

## Slide 18: Effective RowHammer Characterization
To characterize our DRAM chips at worst-case conditions, we:
Prevent sources of interference during core test loop
  We disable:
    DRAM refresh: to avoid refreshing victim row
    DRAM calibration events: to minimize variation in test timing
    RowHammer mitigation mechanisms: to observe circuit-level effects
  Test for less than refresh window (32ms) to avoid retention failures
Worst-case access sequence
- We use worst-case access sequence based on prior works’ observations
- For each row, repeatedly access the two directly physically-adjacent rows as fast as possible
[More details in the paper]
Notes: [CLICK] To characterize our DRAM chips at worst-case conditions we take two measures:
[CLICK] First, we prevent external sources of interference such that the core loop of testing (or the code sequence that repeatedly activates rows) can run consistently as desired and without interruptions
[CLICK] During the core loop of testing, we disable
[CLICK] DRAM refresh so the victim rows are not refreshed during a RowHammer test,
[CLICK] DRAM calibration events to minimize variation in test timings
[CLICK] and RowHammer mitigation mechanisms to ensure that we can directly observe circuit-level bit flips such that we can make conclusions about DRAM vulnerability to RowHammer at the circuit technology level rather than the system level.
[CLICK] we also ensure that the core loop of our test runs for shorter than the refresh window to prevent retention failures from interfering with our results
[CLICK] Second, we try to issue the worst-case access sequence for inducing RowHammer bit flips
[CLICK] we construct the worst-case access sequence based on observations from prior work
[CLICK] Using these observations, we test each row’s worst-case vulnerability to RowHammer by repeatedly accessing the two directly physically-adjacent rows as fast as possible
[CLICK] We refer to our paper for more details on the worst-case access sequence
=========

## Slide 19: Testing Methodology
Row 3
Row 4
Row 3
Row 4
Aggressor Row
Victim Row
Row
Row
Row
Row 5
Row
Row 0
Row 1
Row 2
Row
Row
Row
Row 0
Aggressor Row
Row 2
Aggressor Row
Row 1
Victim Row
REFRESH
Disable refresh to prevent interruptions in the core loop of our test from refresh operations
Induce RowHammer bit flips on a fully charged row
Notes: We describe our RowHammer characterization test using a DRAM diagram and a snippet of pseudocode.
To test each row in DRAM, we run the following sequence
[CLICK] first we set that row as the victim row in which we will induce RowHammer bit flips
[CLICK] we then select the two physically-adjacent rows as aggressor rows which we will repeatedly access
[CLICK] we then disable refresh to prevent interruptions in the core loop of our test from refresh operations
[CLICK] We then refresh the victim row so that we are inducing RowHammer bit flips on a fully charged row and minimizing interference from charge variation in the cells
[CLICK]
=======
HC defined more clearly somewhere

## Slide 20: Testing Methodology
Row 3
Row 4
Row 3
Row 4
Aggressor Row
Victim Row
Row
Row
Row
Row 5
Row
Row 0
Row 1
Row 2
Row
Row
Row
Row 1
Victim Row
Row 2
Aggressor Row
closed
Row 0
Aggressor Row
open
Row 0
Aggressor Row
closed
Row 2
Aggressor Row
open
Row 1
Aggressor Row
Row 3
Aggressor Row
Row 2
Victim Row
Row 2
Aggressor Row
Row 4
Aggressor Row
Row 3
Victim Row
Row 3
Aggressor Row
Row 5
Aggressor Row
Row 4
Victim Row
Row 2
Row
Core test loop where we alternate accesses to adjacent rows
Prevent further retention failures
Record bit flips for analysis
Disable refresh to prevent interruptions in the core loop of our test from refresh operations
Induce RowHammer bit flips on a fully charged row
1 Hammer (HC) = two accesses
Notes: We [FORTH&BACK] then induce RowHammer bit flips in our core test loop by alternating accesses to the aggressor rows
[CLICK] note that 1 hammer, which we call HC, refers to two accesses. One to each of the aggressors
[CLICK] After hammering a prescribed number of times. We then enable DRAM refresh to prevent further retention failures
[CLICK] and record the resulting RowHammer bit flips for analysis
[CLICK] Finally, we restore the bit flips to their original values
[CLICK]
[CLICK] We repeat this sequence for all rows in the DRAM chip
[CLICK]

## Slide 21: Outline
RowHammer Introduction
DRAM Background
Motivation and Goal
Experimental Methodology
Characterization Results
Evaluation of Mitigation Mechanisms
RowHammer Solutions Going Forward
Conclusion
Notes: Now lets go into our characterization results

## Slide 22: Key Takeaways from 1580 Chips
Chips of newer DRAM technology nodes are more vulnerable to RowHammer
There are chips today whose weakest cells fail after only 4800 hammers
Chips of newer DRAM technology nodes can exhibit RowHammer bit flips 1) in more rows and 2) farther away from the victim row.
Notes: Before I go into our detailed results, I will present 3 key takeaways from our experimental charactierzation study of over 1500 chips.
[CLICK] First, chips of newer DRAM technology nodes are more vulnerable to RowHammer
[CLICK] Second, there are chips today whose weakest cells fail after only 4800 hammers
[CLICK] Third, chips of newer DRAM technology nodes can exhibit RowHammer bit flips in more rows and farther away from the victim row
================
People may ask for more data for "farther away from the victim row" (how many rows per aggressor are affected)

## Slide 23: 1. RowHammer Vulnerability
Newer DRAM chips are more vulnerable to RowHammer
Q. Can we induce RowHammer bit flips in all of our DRAM chips?
All chips are vulnerable, except many DDR3 chips
A total of 1320 out of all 1580 chips (84%) are vulnerable
Within DDR3-old chips, only 12% of chips (24/204) are vulnerable
Within DDR3-new chips, 65% of chips (148/228) are vulnerable
27%
11%
85%
92%
0%
0%
Notes: The first question we want to answer is "Can we induce RowHammer bit flips in all of our DRAM chips?"
[CLICK] We find that we are able to induce RowHammer bit flips in all chips we test except many DDR3 DRAM chips
[CLICK] We find that of the total set of chips, 84% are vulnerable. The remaining 16% are of DDR3 DRAM types.
[CLICK] Wtihin DDR3-old chips, we find only 12% of chips to be vulnerable
[CLICK] Within DDR3-new chips, we find 65% of chips to be vulnerable
[CLICK] we conclude that Newer DRAM chips are more vulnerable to RowHammer based on the increasing percentage from DDR3-old to DDR3-new, the fact that all other newer chips are vulnerable, and also as we will show later.
In the remaining characterization results, we only show results for chips that we can induce enough RowHammer bit flips in
====================
Potentially describe the outlier mfr a.

## Slide 24: 2. Data Pattern Dependence
Q. Are some data patterns more effective in inducing RowHammer bit flips?
We test several data patterns typically examined in prior work to identify the worst-case data pattern
The worst-case data pattern is consistent across chips of the same manufacturer and DRAM type-node configuration
We use the worst-case data pattern per DRAM chip to characterize each chip at worst-case conditions and minimize the extensive testing time
[More detail and figures in paper]
Notes: The second question we want to answer is "Are some data patterns more effective in inducing RowHammer bit flips than others?"
[CLICK] We test several data patterns that are typically examined in prior work to identify the worst-case data pattern for inducing RowHammer bit flips
[CLICK] We find that the worst-case data pattern is consistent across chips of the same manufacturer and DRAM type-node configuration
[CLICK] and we use the worst-case data pattern per DRAM chip to characterize each chip at worst-case conditions and minimize the extensive testing time
[CLICK] We refer to our paper for more detail

## Slide 25: 3. Hammer Count (HC) Effects
Q. How does the Hammer Count affect the number of bit flips induced?
Mfr. A DDR4-new
Hammer Count = 2 Accesses,
one to each adjacent row of victim
Notes: The third question we want to answer is "How does the Hammer Count affect the number of bit flips induced?"
[CLICK] We plot the RowHammer bit flip rate (or the number of observed RowHammer bit flips to the total number of bits in the tested DRAM rows) on the y-axis as a function of the hammer count on the x-axis for DDR4-new chips of Mfr A as an example.
[CLICK] Remember that Hammer Count is defined as two accesses. One access to each of the two adjacent rows.

## Slide 26: 3. Hammer Count (HC) Effects
RowHammer bit flip rates (i.e., RowHammer vulnerability)
increase with technology node generation
RowHammer bit flip rates increase
when going from old to new DDR4 technology node generations
Notes: We plot each of these curves across our DRAM type-node configurations per manufacturer
[CLICK] We find that newer DDR4 DRAM technology nodes show a clear trend of increasing RowHammer bit flip rates.
the same Hammer count value causes an increased RowHammer bit flip rate from DDR4-old to DDR4-new DRAM chips of all DRAM manufacturers
[CLICK] This indicates that RowHammer bit flip rates are increasing with newer technology node generations.
=======
spend more time.
Stronger second conclusion. Clear from this that rh bit flips increase with technology node generation. and we show DDR4 as an example.
rowhammer bit flip rates are increasing when going from old to new DDR4 technology nodes.

## Slide 27: 4. Spatial Effects: Row Distance
The number of RowHammer bit flips that occur in a given row decreases as the distance from the victim row (row 0) increases.
Q. Where do RowHammer bit flips occur relative to aggressor rows?
Aggressor Row
Aggressor Row
Mfr. A DDR4-old
Notes: The next question we want to answer is "Where do RowHammer bit flips occur relative to aggressor rows?"
[CLICK] We plot the fraction of RowHammer bit flips that occur in a given row offset from the victim row out of all observed RowHammer bit flips for DDR4-old chips of Mfr A as an example.
[CLICK] The aggressor rows at offsets 1 and -1 are marked and the error bars show the standard deviation of the distribution across our tested chips.
[CLICK] We find that the number of RowHammer bit flips that occur in a given row decreases as the distance from the victim row (or row 0) increases. This is because row 0 is being hammered from both sides with a double-sided hammer, while rows 2 and -2 are only being "hammered" from a single side each.

## Slide 28: 4. Spatial Effects: Row Distance
Chips of newer DRAM technology nodes can exhibit RowHammer
bit flips 1) in more rows and 2) farther away from the victim row.
We normalize data by inducing a bit flip rate of 10-6 in each chip
Notes: We first normalize the data we get across our different chips by inducing a RowHammer bit flip rate of 10-6 in each chip and studying the resulting bit flips
[CLICK] And plot representative distributions for different DRAM type-node configurations ordered from top to bottom
[CLICK] we find that DRAM chips of newer DRAM technology nodes can exhibit RowHammer bit flips in more rows and also farther away from the victim rows.

## Slide 29: 4. Spatial Effects: Row Distance
[More analysis in the paper]
We plot this data for each DRAM type-node configuration per manufacturer
Notes: We plot results for each group of chips from each DRAM type-node configuration per manufacturer in the paper
And we provide more analysis on these results in the paper
====

## Slide 30: 4. Spatial Distribution of Bit Flips
Q. How are RowHammer bit flips spatially distributed across a chip?
The distribution of RowHammer bit flip density per word
changes significantly in LPDDR4 chips from other DRAM types
Representative of DDR3/DDR4 chip
Representative of LPDDR4 chip
We normalize data by inducing a bit flip rate of 10-6 in each chip
At a bit flip rate of 10-6, a 64-bit word can contain up to 4 bit flips.
Even at this very low bit flip rate, a very strong ECC is required
Notes: The next question we want to answer is ”How are RowHammer bit flips spatially distributed across a chip?"
[CLICK] we first normalize the data we get across our different chips by inducing a RowHammer bit flip rate of 10-6 in each chip and studying the resulting bit flips
[CLICK] We plot the distribution of 64-bit words containing x RowHammer bit flips across our tested DRAM chips. We find the proportion of 64-bit words containing x RowHammer bit flips out of all 64-bit words in each chip containing any RowHammer bit flip and plot the distribution as a bar chart with error bars for each x value
[CLICK] we find that this plot is representative of the results from our DDR3 and DDR4 chips.
[CLICK] we next plot data that is representative of our LPDDR4 chips.
[CLICK] We find that the distribution of RowHammer bit flip density per word changes significantly in LPDDR4 chips compared to other DRAM types.
We believe this is due to the interaction of RowHammer bit flips and the on-die ECC that is implemented in the LPDDR4 chips we test.
[CLICK] We find that at a bit flip rate of 10^-6, a 64-bit word can contain up to 4 bit flips. This indicates that even at this relatively low bit flip rate, a DRAM chip can only be protected from RowHammer bit flips with a very strong ECC code
======

## Slide 31: 4. Spatial Distribution of Bit Flips
We plot this data for each DRAM type-node configuration per manufacturer
[More analysis in the paper]
Notes: We show the results for each DRAM type-node configuration per manufacturer as is in the paper.
And we provide more analysis on these plots in the paper

## Slide 32: 5. First RowHammer Bit Flips per Chip
What is the minimum Hammer Count required to cause bit flips (HCfirst)?
Whisker
Q3: 75% point
Median: 50%
Q1: 25% point
Whisker
Notes: We next want to answer the question "What is the minimum hammer count required to cause RowHammer bit flips in a chip?" We refer to this value as HC first
[CLICK] For each DRAM chip we find the lowest number of hammers required to induce a RowHammer bit flip in that chip, and we plot the distribution of those values across each chip in a given DRAM type-node configuration (on the x-axis). We use results from Manufacturer C as an example.
We plot these distribution as box-and-whisker plots, where
[CLICK] the center line indicates the median,
[CLICK] the box edges represent the Q1 and Q3 points,
[CLICK] the whiskers extend 1.5 times the difference between Q3 and Q1 beyond Q3 and Q1 and
[CLICK] Any point outside of the whiskers are outliers and are shown with plus signs.
=======

## Slide 33: 5. First RowHammer Bit Flips per Chip
What is the minimum Hammer Count required to cause bit flips (HCfirst)?
We note the different DRAM types on the x-axis: DDR3, DDR4, LPDDR4.
We focus on trends across chips of the same DRAM type to draw conclusions
Notes: We note the different DRAM types on the x-axis: DDR3, DDR4, and LPDDR4, and subdivide the plots with vertical lines.
We focus on trends across chips of the same DRAM type but different technology node generations to draw conclusions.

## Slide 34: 5. First RowHammer Bit Flips per Chip
Newer chips from a given DRAM manufacturer
more vulnerable to RowHammer
Notes: We plot these distributions across each DRAM manufacturer.
[CLICK] We find that newer chips from a given DRAM manufacturer are more vulnerable to RowHammer, which is demonstrated by the clear reduction in HCfirst values from older to newer DRAM generations across most DRAM types
===============

## Slide 35: 5. First RowHammer Bit Flips per Chip
Newer chips from a given DRAM manufacturer
more vulnerable to RowHammer
There are chips whose weakest cells fail
after only 4800 hammers
In a DRAM type, HCfirst reduces significantly from old to new chips, i.e., DDR3: 69.2k to 22.4k,
DDR4: 17.5k to 10k, LPDDR4: 16.8k to 4.8k
Notes: We plot these distributions across each DRAM manufacturer.
[CLICK] We find that newer chips from a given DRAM manufacturer are more vulnerable to RowHammer, which is demonstrated by the clear reduction in HCfirst values from older to newer DRAM generations across most DRAM types
===============

## Slide 36: Key Takeaways from 1580 Chips
Chips of newer DRAM technology nodes are more vulnerable to RowHammer
There are chips today whose weakest cells fail after only 4800 hammers
Chips of newer DRAM technology nodes can exhibit RowHammer bit flips 1) in more rows and 2) farther away from the victim row.
Notes: To reiterate our three key takeaways from our experimental characterization, we find that
[CLICK] First, chips of newer DRAM technology nodes are more vulnerable to RowHammer
[CLICK] Second, there are chips today whose weakest cells fail after only 4800 hammers
[CLICK] Third, chips of newer DRAM technology nodes can exhibit RowHammer bit flips in more rows and farther away from the victim row
================

## Slide 37: Outline
RowHammer Introduction
DRAM Background
Motivation and Goal
Experimental Methodology
Characterization Results
Evaluation of Mitigation Mechanisms
RowHammer Solutions Going Forward
Conclusion
Notes: I will next present our evaluation of mitigation mechanisms after first explaining our evaluation methodology

## Slide 38: Evaluation Methodology
Cycle-level simulator: Ramulator [Kim+, CAL’15] https://github.com/CMU-SAFARI/ramulator
  4GHz, 4-wide, 128 entry instruction window
  48 8-core workload mixes randomly drawn from SPEC CPU2006 (10 < MPKI < 740)
Metrics to evaluate mitigation mechanisms
  DRAM Bandwidth Overhead: fraction of total system DRAM bandwidth consumption from mitigation mechanism
  Normalized System Performance: normalized weighted speedup to a 100% baseline
Notes: [CLICK] We use ramulator, a cycle-level DRAM simulator with a simple core model to examine 48 8-core workload mixes drawn from SPEC CPU2006 with last level cache misses per kilo-instruction or MPKI values ranging between 10 and 740. We note that there could be other workloads with which mitigation mechanisms exhibit higher performance overheads, but we did not try to maximize the overhead experienced by workloads by biasing the workload construction in any way.
[CLICK] We use two metrics to evaluate our mechanisms
[CLICK] First, we use DRAM Bandwidth overhead, which is the fraction of the total system DRAM bandwidth consumption coming from the RowHammer mitigation mechanism
[CLICK] Second, we use Normalized System Performance, which is the weighted speedup metric normalized to the baseline value, which we denote as 100%. We find that when using RowHammer mitigation mechanisms, most values appear below the baseline. Therefore, for clarity, we refer to normalized weighted speedup as normalized system performance in our evaluations
[CLICK] While we present the results of both metrics in the paper, we focus on our Normalized system performance results in this talk as they are highly correlated
==================

## Slide 39: Evaluation Methodology
We evaluate five state-of-the-art mitigation mechanisms:
  Increased Refresh Rate [Kim+, ISCA’14]
  PARA [Kim+, ISCA’14]
  ProHIT [Son+, DAC’17]
  MRLoc [You+, DAC’19]
  TWiCe [Lee+, ISCA’19]
and one ideal refresh-based mitigation mechanism:
  Ideal
More detailed descriptions in the paper on:
  Descriptions of mechanisms in our paper and the original publications
  How we scale each mechanism to more vulnerable DRAM chips (lower HCfirst)
Notes: [CLICK] We evaluate five state-of-the-art mitigation mechanisms
[CLICK] and one ideal refresh-based mitigation mechanism
[CLICK] Please refer to our paper and the respective original publications for more detailed descriptions of each mechanism, and how we scale each mechanism to DRAM chips that are more vulnerable to RowHammer or that require a lower hammer count to induce the first RowHammer bit flip in the chip. As a reminder, we refer to this value as HCfirst
===========

## Slide 40: Mitigation Mech. Eval. (Increased Refresh)
105
104
103
102
105
104
103
102
HCfirst (number of hammers required to induce first RowHammer bit flip)
Increased Refresh Rate
Substantial overhead for high HCfirst values.
This mechanism does not support HCfirst < 32k
due to the prohibitively high refresh rates required
Notes: We plot normalized system performance as a function of HCfirst, or the number of hammers required to induce the first RowHammer bit flip in a chip. A Lower y value corresponds to worse system performance and we sweep HCfirst between 200k and 64.
[CLICK] We first plot the results for the increased refresh rate mechanism.
[CLICK] we note that there is substantial overhead even at high HCfirst values and that it does not scale under HCfirst values of 32k due to prohibitively high refresh rates required for mitigating RowHammer bit flips.
========
Title mention the mechanism evaluated

## Slide 41: Mitigation Mechanism Evaluation (PARA)
105
104
103
102
105
104
103
102
PARA
HCfirst (number of hammers required to induce first RowHammer bit flip)
Low Performance Overhead
High Performance Overhead
80% performance loss
Notes: We next plot the results for PARA and find that it [CLICK] results in reasonable normalized system performance until around the point where HCfirst is 4000, at which point the system performance quickly reduces.
[CLICK] When HCfirst is 128, the system suffers 80% performance loss

## Slide 42: Mitigation Mechanism Evaluation (ProHIT)
105
104
103
102
105
104
103
102
PARA
ProHIT
HCfirst (number of hammers required to induce first RowHammer bit flip)
Notes: We next plot ProHIT

## Slide 43: Mitigation Mechanism Evaluation (MRLoc)
105
104
103
102
105
104
103
102
PARA
MRLoc
HCfirst (number of hammers required to induce first RowHammer bit flip)
Models for scaling ProHIT and MRLoc for HCfirst < 2k
are not provided and how to do so is not intuitive
Supported
Not supported
Notes: and MRLoc for a single data point of HCfirst = 2000.[CLICK] We only plot a single data point, since both of these works do not provide models for scaling their mechanisms to lower HCfirst values and how to do so is not intuitive.

## Slide 44: Mitigation Mechanism Evaluation (TWiCe)
105
104
103
102
105
104
103
102
PARA
TWiCe-ideal
TWiCe
HCfirst (number of hammers required to induce first RowHammer bit flip)
Supported
Not supported
TWiCe does not support HCfirst < 32k.
We evaluate an ideal scalable version (TWiCe-ideal)
assuming it solves two critical design issues
Notes: We next plot the results for TWiCe with a solid line, which has high normalized system performance for HCfirst values that it supports.
[CLICK] In its current form, TWiCe does not support HCfirst values under 32k, but we evaluate an ideal version that we refer to as TWiCe-ideal assuming that it solves two critical design issues in scaling. TWiCe-ideal is drawn with a dashed line. We note that TWiCe-ideal has the potential to provide a higher normalized system performance compared to PARA for all HCfirst values, but only if it is able to overcome the critical design issues. We discuss these issues in more detail in the paper
==========

## Slide 45: Mitigation Mechanism Evaluation (Ideal)
105
104
103
102
105
104
103
102
PARA
TWiCe-ideal
Ideal
HCfirst (number of hammers required to induce first RowHammer bit flip)
Ideal mechanism issues a refresh command
to a row only right before the row
can potentially experience a RowHammer bit flip
6% performance loss
Notes: We next plot the ideal refresh-based mitigation mechanism in green.
[CLICK] The ideal mechanism works by tracking every single activation and issuing a refresh command to a row only right before it can potentially experience a RowHammer bit flip.
We find that the ideal mechanism provides reasonably high normalized system performance across all tested HCfirst values. However, there is still opportunity for exceeding the scalability of the ideal refresh-based mechanism, which [CLICK] results in 6% performance loss when HCfirst is 128.
====

## Slide 46: Mitigation Mechanism Evaluation
105
104
103
102
105
104
103
102
DDR3-old
DDR3-new
DDR4-old
LPDDR4-1x
DDR4-new
LPDDR4-1y
PARA
TWiCe-ideal
Ideal
PARA, ProHIT, and MRLoc mitigate RowHammer bit flips
in worst chips today with reasonable system performance (92%, 100%, 100%)
HCfirst (number of hammers required to induce first RowHammer bit flip)
Notes: [CLICK] We next overlay the lowest HCfirst values observed across all chips of a given DRAM type-node configuration, to show exactly how each mechanism would affect a system's performance when used on a system using a particular DRAM type-node configuration
[CLICK] We find that PARA, ProHIT and MRLoc are viable options for mitigating RowHammer bit flips in the worst chips that we tested today with reasonable system performance

## Slide 47: Mitigation Mechanism Evaluation
105
104
103
102
105
104
103
102
DDR3-old
DDR3-new
DDR4-old
LPDDR4-1x
DDR4-new
LPDDR4-1y
PARA
TWiCe-ideal
Ideal
Only PARA’s design scales to low HCfirst values
but has very low normalized system performance
HCfirst (number of hammers required to induce first RowHammer bit flip)
Notes: However, only PARA’s design scales to low HCfirst values that we are likely to see in future DRAM chips but has very low normalized system performance

## Slide 48: Mitigation Mechanism Evaluation
105
104
103
102
105
104
103
102
DDR3-old
DDR3-new
DDR4-old
LPDDR4-1x
DDR4-new
LPDDR4-1y
PARA
TWiCe-ideal
Ideal
Ideal mechanism is significantly better
than any existing mechanism for HCfirst < 1024
Significant opportunity for developing a RowHammer solution
with low performance overhead that supports low HCfirst
HCfirst (number of hammers required to induce first RowHammer bit flip)
Notes: We find that the ideal refresh-based mitigation mechanism is significantly better than any existing mechanism as HCFirst reduces below 1024 .
[CLICK] And this indicates significant opportunity for developing a RowHammer solution with low performance overhead that also scales to low HCFirst values

## Slide 49: Key Takeaways from Mitigation Mechanisms
Existing RowHammer mitigation mechanisms can prevent RowHammer attacks with reasonable system performance overhead in DRAM chips today
Existing RowHammer mitigation mechanisms do not scale well to DRAM chips more vulnerable to RowHammer
There is still significant opportunity for developing a mechanism that is scalable with low overhead
Notes: From our evaluation of mitigation mechanisms
[CLICK] we find that existing RowHammer mitigation mechanisms can prevent RowHammer attacks with reasonable system performance overhead in DRAM chips today
[CLICK] However, existing mitigation mechanisms do not scale well to DRAM chips that are more vulnerable to RowHammer
[CLICK] and there is still significant opportunity for developing a mechanism that is scalable with low overhead
===========

## Slide 50: Additional Details in the Paper
Single-cell RowHammer bit flip probability
More details on our data pattern dependence study
Analysis of Error Correcting Codes (ECC) in mitigating RowHammer bit flips
Additional observations on our data
Methodology details for characterizing DRAM
Further discussion on comparing data across different infrastructures
Discussion on scaling each mitigation mechanism
Notes: There are additional details in the paper including:
[CLICK] a study on the single-cell RowHammer bit flip probability
[CLICK] more details on our data pattern dependence study
[CLICK] an analysis of Error Correcting Codes (ECC) in mitigating RowHammer bit flips
[CLICK] additional observations on our data
[CLICK] methodology details for characterizing DRAM
[CLICK] further discussion on comparing data across different infrastructures and a
[CLICK] discussion on scaling each mitigation mechanism
=======

## Slide 51: Outline
RowHammer Introduction
DRAM Background
Motivation and Goal
Experimental Methodology
Characterization Results
Evaluation of Mitigation Mechanisms
RowHammer Solutions Going Forward
Conclusion
Notes: To develop a scalable and low-overhead mechanism that can prevent RowHammer bit flips in DRAM chips with a high
degree of RowHammer vulnerability we believe it is essential to explore all possible avenues for RowHammer mitigation.

## Slide 52: RowHammer Solutions Going Forward
Two promising directions for new RowHammer solutions:
DRAM-system cooperation
  We believe the DRAM and system should cooperate more to provide a holistic solution can prevent RowHammer at low cost
Profile-guided
  Accurate profile of RowHammer-susceptible cells in DRAM provides a powerful substrate for building targeted RowHammer solutions, e.g.:
    Only increase the refresh rate for rows containing RowHammer-susceptible cells
  A fast and accurate profiling mechanism is a key research challenge for developing low-overhead and scalable RowHammer solutions
Notes: We identify two promising directions for new RowHammer solutions
[CLICK] First, we believe that the [CLICK] DRAM and system should cooperate more to provide a holistic approach that can prevent RowHammer at low cost
[CLICK] Second, we believe that a profile-guided approach can provide significant benefits.
[CLICK] Accurately profiling RowHammer-susceptible cells in DRAM provides a powerful substrate for building target RowHammer solutions. For Example:
[CLICK] in the Increasing refresh rate mechanism, the DRAM bandwidth overhead could be reduced by only increasing the refresh rate for rows containing RowHammer-susceptible cells
[CLICK] We believe that a fast and accurate profiling mechanism is a key research challenge for developing low-overhead and scalable RowHammer solutions
=============
[CLICK] In mechanisms that use DRAM access counters, we could lower the area overhead by only counting accesses to rows containing RowHammer-susceptible cells.
beautify. Maybe reduce and save time. DRAM system should cooperate more. Details in the paper

## Slide 53: Outline
RowHammer Introduction
DRAM Background
Motivation and Goal
Experimental Methodology
Characterization Results
Evaluation of Mitigation Mechanisms
RowHammer Solutions Going Forward
Conclusion
Notes: Now that i've presented all of our results, let me conclude

## Slide 54: Conclusion
We characterized 1580 DRAM chips of different DRAM types, technology nodes, and manufacturers.
We studied five state-of-the-art RowHammer mitigation mechanisms and an ideal refresh-based mechanism
We made two key observations
  RowHammer is getting much worse. It takes much fewer hammers to induce RowHammer bit flips in newer chips
    e.g., DDR3: 69.2k to 22.4k, DDR4: 17.5k to 10k, LPDDR4: 16.8k to 4.8k
  Existing mitigation mechanisms do not scale to DRAM chips that are more vulnerable to RowHammer
    e.g., 80% performance loss when the hammer count to induce the first bit flip is 128
We conclude that it is critical to do more research on RowHammer and develop scalable mitigation mechanisms to prevent RowHammer in future systems
Notes: We characterized over 1500 DRAM chips of different DRAM types, technology nodes and manufacturers
[CLICK] we studied five state-of-the-art RowHammer mitigation mechanisms and an ideal refresh-based mechanism
[CLICK] and we made two key observations.
[CLICK] First, RowHAmmer is getting much worse. It takes much fewer hammers to induce RowHAmmer bit flips in newer chips
[CLICK] Second, existing mitigation mechanisms do not scale to DRAM chips that are more vulnerable to RowHammer
[CLICK] we conclude that it is critical to do more research on RowHammer and develop scalable mitigation mechanisms to prevent RowHammer in future systems
=====

## Slide 55
Jeremie S. Kim Minesh Patel
A. Giray Yağlıkçı Hasan Hassan
Roknoddin Azizi Lois Orosa Onur Mutlu
Revisiting RowHammer An Experimental Analysis of Modern Devices and Mitigation Techniques
Notes: This concludes my talk . Thank you for your time and attention. For many more details, I invite you to read our ISCA 2020 paper.

## Slide 56: Evaluation
105
104
103
102
105
104
103
102
HCfirst
DDR3-old
DDR3-new
DDR4-old
LPDDR4-1x
DDR4-new
LPDDR4-1y
DDR3-old
DDR3-new
DDR4-old
LPDDR4-1x
DDR4-new
LPDDR4-1y
PARA
PARA
TWiCe-ideal
TWiCe-ideal
Ideal
Ideal

## Slide 57: Mitigation Mechanism Evaluation
105
104
103
102
105
104
103
102
HCfirst
Does not scale for HCfirst values < 32k
due to significantly high refresh rates
Substantial overhead even at high HCfirst values
Increased Refresh Rate
Increased Refresh Rate
Notes: We plot our two metrics as functions of HCfirst, or the number of hammers required to induce the first RowHammer bit flip in a chip. The top figure plots the DRAM bandwdith overhead as a percentage with an inverse log y-axis and the bottom figure plots the normalized system performance as a percentage. In both figures, lower is worse. We sweep HCfirst between 200k and 64.
[CLICK] We first plot the increased refresh rate in both plots.
[CLICK] we note that there is substantial overhead even at high HCfirst values and that it does not scale under HCfirst values of 32k due to significantly high refresh rates required for mitigating RowHammer bit flips.
=======================
Maybe just show the performance figure . Maybe just in the longer version of the talk. We evaluate two things but we focus on the bottom figure.

## Slide 58: Mitigation Mechanism Evaluation
105
104
103
102
105
104
103
102
HCfirst
PARA
PARA
Notes: We next plot the results for PARA and find that it results in reasonable normalized system performance until around the point where HCfirst is 4000, at which point the system performance quickly reduces.

## Slide 59: Mitigation Mechanism Evaluation
105
104
103
102
105
104
103
102
HCfirst
PARA
PARA
ProHIT
Notes: We next plot ProHIT

## Slide 60: Mitigation Mechanism Evaluation
105
104
103
102
105
104
103
102
HCfirst
PARA
PARA
MRLoc
MRLoc
Notes: and MRLoc for a single data point of HCfirst = 2000.We only plot a single data point, since both of these works do not provide models for scaling their mechanisms to lower HCfirst values and how to do so is not intuitive.
======================
remind people what HCfirst is on slide (parenthesis).
When describing different mechanisms, mark points of overhead when talking about them.

## Slide 61: Mitigation Mechanism Evaluation
105
104
103
102
105
104
103
102
HCfirst
PARA
PARA
TWiCe-ideal
TWiCe-ideal
TWiCe’s current form does not support HCfirst < 32k, but we evaluate an ideal version (TWiCe-ideal) assuming it solves two critical design issues
TWiCe
TWiCe
Notes: We next plot the results for TWiCe, which has high normalized system performance for HCfirst values that it supports.
[CLICK] In its current form, TWiCe does not support HCfirst values under 32k, but we evaluate an ideal version that we refer to as TWiCe-ideal assuming that it solves two critical design issues in scaling. TWiCe-ideal is drawn with a dashed line. We note that TWiCe-ideal has the potential to provide a higher normalized system performance compared to PARA for all HCfirst values, but only if it is able to overcome the critical design issues.

## Slide 62: Mitigation Mechanism Evaluation
105
104
103
102
105
104
103
102
HCfirst
DDR3-old
DDR3-new
DDR4-old
LPDDR4-1x
DDR4-new
LPDDR4-1y
DDR3-old
DDR3-new
DDR4-old
LPDDR4-1x
DDR4-new
LPDDR4-1y
PARA
PARA
TWiCe-ideal
TWiCe-ideal
Ideal
Ideal
Notes: We next plot the ideal refresh-based mitigation mechanism in green. We find that the ideal mechanism provides reasonably high normalized system performance across all tested HCfirst values. However, there is still opportunity for exceeding the scalability of the ideal refresh-based mechanism, which results in 6% performance loss when HCfirst is 128.
[CLICK] We next overlay the lowest HCfirst values observed across all chips of a given DRAM type-node configuration, to show exactly how each mechanism would affect a system's performance when used on a system using a particular DRAM type-node configuration

## Slide 63: Mitigation Mechanism Evaluation
105
104
103
102
HCfirst
DDR3-old
DDR3-new
DDR4-old
LPDDR4-1x
DDR4-new
LPDDR4-1y
DDR3-old
DDR3-new
DDR4-old
LPDDR4-1x
DDR4-new
LPDDR4-1y
PARA
PARA
TWiCe-ideal
TWiCe-ideal
Ideal
Ideal
105
104
103
102
PARA, ProHIT, and MRLoc are viable options
for mitigating RowHammer bit flips in worst chips today
with reasonable system performance (92%, 100%, 100%)
Notes: We find that PARA, ProHIT, and MRLoc are viable options for mitigation RowHammer bit flips in the worst chips we test with reasonable system performance.

## Slide 64: Mitigation Mechanism Evaluation
105
104
103
102
HCfirst
DDR3-old
DDR3-new
DDR4-old
LPDDR4-1x
DDR4-new
LPDDR4-1y
DDR3-old
DDR3-new
DDR4-old
LPDDR4-1x
DDR4-new
LPDDR4-1y
PARA
PARA
TWiCe-ideal
TWiCe-ideal
Ideal
Ideal
105
104
103
102
Only PARA’s design scales to low HCfirst values
that we may see in future DRAM chips but
has very low normalized system performance
Notes: However, across all existing RowHammer mitigation mechanisms, only PARA's design scales to low HCfirst values that we may see in future DRAM chips, but significantly affects the system performance at low HCfirst values

## Slide 65: Mitigation Mechanism Evaluation
105
104
103
102
HCfirst
DDR3-old
DDR3-new
DDR4-old
LPDDR4-1x
DDR4-new
LPDDR4-1y
DDR3-old
DDR3-new
DDR4-old
LPDDR4-1x
DDR4-new
LPDDR4-1y
PARA
PARA
TWiCe-ideal
TWiCe-ideal
Ideal
Ideal
105
104
103
102
The ideal refresh-based mitigation mechanism
is significantly better than any existing mechanism
as HCfirst reduces below 1024
This indicates significant opportunity for developing
a RowHammer solution with low performance overhead that also scales to low HCfirst values
Notes: The ideal refresh-based mitigation mechanism is significantly better than any existing mechanism as HCfirst reduces below 1024.
[CLICK] This indicates signifcant opportunity for developing a RowHammer solution with low performance overhead that also scales to low HCfirst values
==========
optimize these mitigation mechanisms.

## Slide 66: History of RowHammer
DDR3
DDR4
LPDDR4
2020 - Our Work
2014 - First RowHammer publication
????

## Slide 67
DRAM Bank
local
bitline
wordline
DRAM cell
DRAM row
A DRAM bank is hierarchically organized into subarrays
Columns of cells in subarrays share a local bitline
Rows of cells in a subarray share a wordline
DRAM Organization
Notes: [CLICK] Each DRAM bank is hierarchically organized into subarrays. [CLICK] Each circle in the cartoon represents a single DRAM cell. [CLICK] columns of DRAM cells in a subarray are connected with a wire referred to as a local bitline. [CLICK] and rows of DRAM cells are connected with a wire referred to as a wordline, and [CLICK] a row of DRAM cells is called a DRAM row. [CLICK] at the peripherals of the core cell arrays are a local row decoder, which selects the row to read and write to, and a local row-buffer which amplifies the data that is stored in the cell to an I/O readable value. [CLICK] DRAM is comprised of many subarrays which are often composed of 512 to 1024 rows. [CLICK] Further peripherals exist containing groups of subarrays called [CLICK] a bank. The global row decoder selects the local row decoder that will drive the wordline, and global row buffer aids in the transfer of data to and from the CPU. A DRAM device is comprised of several banks, and each bank can be accessed independently [CLICK]

## Slide 68
DRAM Operation
…
…
…
…
…
Local Row Buffer
Local Row Buffer
Cache line
READ
…
READ
READ
Row Decoder
Local Row Buffer
READ
READ
READ
ACT R0
RD
PRE R0
RD
RD
ACT R1
RD
RD
RD
time
DRAM Command Sequence
Notes: Let’s take a look at how DRAM operates in the scope of a single subarray. [CLICK] Because memory controllers typically access DRAM at the granularity of a cache line, we combine consecutive, aligned DRAM cells as cache lines in our diagram. [CLICK] First, we activate the first row, which [CLICK] copies the entire rows' data into the row buffer. At this point, we can [CLICK] read our data at the granularity [CLICK] of cache lines within the [CLICK] activated or opened row. When we want to access data on another row, we must precharge [CLICK] the currently opened row, which prepares the row buffer for copying data from another row. We can now [CLICK] activate the second row, before reading data from it [CLICK][CLICK][CLICK]

## Slide 69: Characterization Results
RowHammer Vulnerability of DRAM chips we test
Data Pattern Dependence of RowHammer bit flips
Hammer Count effects on RowHammer bit flips
Spatial Analysis on RowHammer bit flips
First RowHammer Bit Flips per device
Error Correcting Codes in RowHammer mitigation
Notes: [CLICK] First, we study whether the DRAM chips we have are vulnerable to RowHammer under our testing conditions
[CLICK] Second, we study the effect of storing different data patterns in DRAM on the number of RowHammer bit flips induced
[CLICK] Third, we study the effects of changing the number of times we hammer DRAM on the number of RowHammer bit flips induced
[CLICK] Fourth, we analyze the spatial distributions of RowHammer bit flips that we induce
[CLICK] Fifth, we examine each chip’s lowest hammer count required to induce the first RowHammer bit flip.
[CLICK] Sixth, we examine the effectiveness of error correcting codes in mitigating RowHammer bit flips
==============
remove this slide . fix color on 6. we talked about X but others are in the paper.

## Slide 70: 1. RowHammer Vulnerability
Newer DRAM chips appear to be more vulnerable to RowHammer
Can we induce RowHammer bit flips in all of our DRAM chips?
We are able to induce RowHammer bit flips in all chips we test except many DDR3 DRAM chips
We only show results
for chips that we can induce
enough RowHammer bit flips in
Notes: Newer DRAM chips appear to be more vulnerable to RowHammer based on the increasing fraction of RowHammerable chips from DDR3-old to DDR3-new DRAM chips of manufacturers B and C.
We only show results
for chips that we can induce
enough RowHammer bit flips in

## Slide 71: Evaluated Mitigation Mechanisms
Five state-of-the-art mitigation mechanisms:
Increased Refresh Rate [Kim+, ISCA’14]: Refresh at a high enough rate such that RowHammer bit flips do not occur
PARA [Kim+, ISCA’14]: Every time a row is opened and closed, PARA refreshes adjacent rows with a low probability
ProHIT [Son+, DAC’17]: Probabilistically manages “Hot” and “Cold” tables to track frequently activated rows to refresh victim rows
MRLoc [You+, DAC’19]: Estimates activation rates via queue and probabilistically refreshes based on estimated activation rate
TWiCe [Lee+, ISCA’19]: Uses tables with lifetime counter and activation counter to determine activation rate and prunes table to minimize overhead according to an activation rate threshold
One ideal refresh-based mitigation mechanism:
Ideal Refresh-based: Issues a refresh command to a row only right before it can potentially experience a RowHammer bit flip.
[More detailed descriptions in the paper]
Notes: [CLICK] We evaluate five state-of-the art mitigation mechanisms
[CLICK] We evaluate a mechanism that we refer to as Increased Refresh Rate. This mechanism works by increasing the overall DRAM refresh rate such that it is impossible to issue enough activations within one refresh window (or the time between two consecutive refresh commands to a single DRAM row) to any single DRAM row to induce a RowHammer bit flip.
[CLICK] PARA is a mechanism that every time a row is opened and closed, refreshes adjacent rows with a low probability
[CLICK] ProHIT probabilistically manages hot and cold tables to track frequently activated rows and refreshes potential victim rows before RowHammer bit flips are induced
[CLICK] MRLoc estimates activation rates with a queue that tracks DRAM activations and probabilistically refreshes victim rows based on an estimated activation rate of aggressor rows
[CLICK] TWiCe uses tables with a lifetime counter and activation counter to determine activation rate and prunes the tables to minimize overhead according to an activation rate threshold
[CLICK] We also evaluate an ideal refresh-based mitigation mechanism [CLICK] that is able to track every DRAM activation to every row and issues a refresh command to a victim row only if the aggressor rows are just about to be activated enough times to induce a RowHammer bit flip.
[CLICK] we refer the interested listener to our paper and the prior work for more detailed descriptions on each mechanism
=============
maybe not describe these. Talk about these less. We selected these out of our analysis.

## Slide 72: 2. Data Pattern Dependence
Testing with different data patterns is essential
for comprehensively identifying RowHammer bit flips
Q. Are some data patterns more effective in inducing RowHammer bit flips?
Notes: The second question we want to answer is "Are some data patterns more effective in inducing RowHammer bit flips than others?"
[CLICK] For each data pattern that we test (on the x-axis), we plot the percentage of unique RowHammer bit flips found by that data pattern out of the total set of unique RowHammer bit flips found by all data patterns.
[CLICK] We find that testing with different data patterns is essential for comprehensively identifying RowHammer bit flips, because no individual data pattern achieves full coverage alone

## Slide 73: 2. Data Pattern Dependence
The worst-case data pattern is consistent across chips
of the same manufacturer and DRAM type-node configuration
Notes: We plot this data across all DRAM chips split into DRAM type-node configurations across each manufacturer.
[CLICK] We find that the worst-case data pattern is consistent across chips of the same manufacturer and DRAM type-node configurations.

## Slide 74: 2. Data Pattern Dependence
The worst-case data pattern is consistent across chips of the same manufacturer and DRAM type-node configuration
We use the worst-case data pattern
per DRAM chip to characterize each chip
at worst-case conditions
and minimize the extensive testing time
Notes: In the remaining experiments, we use the worst-case data pattern per DRAM chip to characterize each chip at worst-case conditions and minimize the extensive testing time

## Slide 75: Effective RowHammer Characterization
To characterize our DRAM chips at worst-case conditions, we:
Prevent sources of interference during core test loop
  We disable: DRAM refresh, DRAM calibration events, RowHammer mitigation mechanisms
  Ensure test shorter than refresh window (i.e., 32ms) to prevent retention failures
Worst-case access sequence
We construct based on three observations from prior work:
An aggressor row causes the most RowHammer bit flips in immediately adjacent rows
A double-sided hammer targeting victim row N (i.e., repeatedly accessing rows N+1 and N-1) causes the most bit flips in row N compared to other access patterns
Increasing the rate of DRAM activations results in more RowHammer bit flips
  Using these observations, we test each row’s worst-case vulnerability to RowHammer by repeatedly accessing the two directly
  physically-adjacent rows as fast as possible
Notes: [CLICK] To characterize our DRAM chips at worst-case conditions we take two measures:
[CLICK] First, we prevent external sources of interference such that the core loop of testing (or the code sequence that repeatedly activates rows) can run consistently as desired and without interruptions
[CLICK] During the core loop of testing, we disable DRAM refresh, DRAM calibration events, and RowHammer mitigation mechanisms
[CLICK] we also ensure that the core loop of our test runs for shorter than the refresh window to prevent retention failures from interfering with our results
[CLICK] Second, we try to issue the worst-case access sequence for inducing RowHammer bit flips
[CLICK] We construct our access sequence using three observations from prior work:
[CLICK] First, an aggressor row causes the most RowHammer bit flips in immediately adjacent rows
[CLICK] Second, a double-sided hammer targeting victim row N (i.e., repeatedly accessing rows N+1 and N-1) causes the most bit flips in row N compared to other access patterns
[CLICK] Third, Increasing the rate of DRAM activations results in more RowHAmmer bit flips
[CLICK] Using these observations, we test each row’s worst-case vulnerability to RowHammer by repeatedly accessing the two directly physically-adjacent rows as fast as possible

## Slide 76: 6. Error-Correcting Code (ECC) Effects
Q. How would different Error Correction Codes (ECC) change
the Hammer Count required to cause RowHammer bit flips?
Notes: We next want to answer the question "How would different Error correcting codes or ECCs change the Hammer Count required to cause RowHammer bit flips?
We plot as a bar graph the hammer count required to find the first 64-bit word containing one- two- and three RowHammer bit flips (indicated on the x-axis). The error bars represent the standard deviation of HC values across all chips tested. On the same plot, we draw with red boxplots, the increase in hammer count (on the right y-axis) between the hammer counts required to find the first 64-bit word containing one and two RowHammer bit flips and two and three RowHammer bit flips. These multipliers indicate how HCfirst would change in a chip if the chip uses single-error correcting ECC, or moves from a single-error correcting to a double-error correcting ECC.

## Slide 77: 6. Error-Correcting Code (ECC) Effects
Single-error correcting code can improve HCfirst by up to 2.78× in DDR4 DRAM chips, and 1.65× in DDR3-new DRAM chips.
Notes: We plot this across all DRAM type-node configurations per DRAM manufacturer
[CLICK] We find that single-error correcting codes can improve HCfirst by up to 2.78x in DDR4 DRAM chips and 1.65x in DDR3-new DRAM chips.
We also note that moving from a double-error correcting code to a triple-error correcting code has diminishing returns in DDR4-old and DDR4-new DRAM chips compared to when moving from a single-error correcting code to a double-error correcting code. However, using a triple-error correcting code in DDR3-new DRAM chips continues to further improve the HCfirst and thus reduce the DRAM chips’ vulnerability to RowHammer.

## Slide 78: RowHammer Solutions Going Forward
Two promising directions for new RowHammer solutions:
DRAM-system cooperation
  DRAM-based or system-level mechanism alone ignores potential benefits of addressing the RowHammer vulnerability holistically
  We believe a holistic solution can prevent RowHammer at low cost
Profile-guided
  Accurate profile of RowHammer-susceptible cells in DRAM provides a powerful substrate for building targeted RowHammer solutions, e.g.:
    Only increase the refresh rate for rows containing RowHammer-susceptible cells
  We believe a fast and accurate profiling mechanism is a key research challenge for developing low-overhead and scalable RowHammer solutions
Notes: We identify two promising directions for new RowHammer solutions
[CLICK] First, we believe that a mechanism that provides higher cooperation between the DRAM chip and the rest of the system can provide many benefits.
[CLICK] using a DRAM-based or system-level mechanism alone ignores potential benefits of addressing the RowHammer vulnerability holistically
[CLICK] We believe that a more holistic approach can achieve a high degree of protection at low cost
[CLICK] Second, we believe that a profile-guided approach can provide significant benefits.
[CLICK] Accurately profiling RowHammer-susceptible cells in DRAM provides a powerful substrate for building target RowHammer solutions. For Example:
[CLICK] in the Increasing refresh rate mechanism, the DRAM bandwidth overhead could be reduced by only increasing the refresh rate for rows containing RowHammer-susceptible cells
[CLICK] We believe that a fast and accurate profiling mechanism is a key research challenge for developing low-overhead and scalable RowHammer solutions
=============
[CLICK] In mechanisms that use DRAM access counters, we could lower the area overhead by only counting accesses to rows containing RowHammer-susceptible cells.
beautify. Maybe reduce and save time. DRAM system should cooperate more. Details in the paper