## Slide 1
Understanding Reduced-Voltage Operation in Modern DRAM Devices
Kevin Chang†
A. Giray Yaglikci†, Saugata Ghose†, Aditya Agrawal*, Niladrish Chatterjee*, Abhijith Kashyap†, Donghyuk Lee*, Mike O’Connor*, Hasan Hassan‡, Onur Mutlu†‡
Experimental Characterization, Analysis, and Mechanisms
†
*
‡

## Slide 2: Executive Summary
DRAM (memory) power is significant in today’s systems
  Existing low-voltage DRAM reduces voltage conservatively
Goal: Understand and exploit the reliability and latency behavior of real DRAM chips under aggressive reduced-voltage operation
Key experimental observations:
  Errors occur and increase with lower voltage
  Errors exhibit spatial locality
  Higher operation latency mitigates voltage-induced errors
Voltron: A new DRAM energy reduction mechanism
  Reduce DRAM voltage without introducing errors
  Use a regression model to select voltage that does not degrade performance beyond a chosen target  7.3% system energy reduction

## Slide 3: Outline
Executive Summary
Motivation
DRAM Background
Characterization of DRAM
Voltron: DRAM Energy Reduction Mechanism
Conclusion

## Slide 4: High DRAM Power Consumption
Problem: High DRAM (memory) power in today’s systems
>40% in POWER7 (Ware+, HPCA’10)
  >40% in GPU (Paul+, ISCA’15)

## Slide 5: Low-Voltage Memory
Existing DRAM designs to help reduce DRAM power by lowering supply voltage conservatively
DDR3L (low-voltage) reduces voltage from 1.5V to 1.35V (-10%)
LPDDR4 (low-power) employs low-power I/O interface with 1.2V (lower bandwidth)
Can we reduce DRAM power and energy by further reducing supply voltage?

## Slide 6: Goals
1 Understand and characterize the various characteristics of DRAM under reduced voltage
2 Develop a mechanism that reduces DRAM energy by lowering voltage while keeping performance loss within a target

## Slide 7: Key Questions
How does reducing voltage affect reliability (errors)?
How does reducing voltage affect DRAM latency?
How do we design a new DRAM energy reduction mechanism?

## Slide 8: Outline
Executive Summary
Motivation
DRAM Background
Characterization of DRAM
Voltron: DRAM Energy Reduction Mechanism
Conclusion

## Slide 9: High-Level DRAM Organization
DRAM
Channel
DRAM Module
DRAM chips

## Slide 10: DRAM Chip Internals
Control Logic
I/O
Peripheral Circuitry
Bitline
S
S
S
S
Sense amplifiers
(row buffer)
Wordline
DRAM Cell
Bank
DRAM Array
Off-chip channel

## Slide 11: DRAM Operations
ACTIVATE: Store the row into the row buffer
READ: Select the target cache line and drive to CPU
PRECHARGE: Prepare the array for a new ACTIVATE
1
1
1
1
1
2
3
to I/O

## Slide 12: DRAM Access Latency
Command
Data
Duration
ACTIVATE
READ
PRECHARGE
1
1
1
1
Cache line (64B)
Next
ACT
Activation latency (13ns / 50 cycles)
1
Precharge latency (13ns / 50 cycles)
2

## Slide 13: Outline
Executive Summary
Motivation
DRAM Background
Characterization of DRAM
  Experimental methodology
  Impact of voltage on reliability and latency
Voltron: DRAM Energy Reduction Mechanism
Conclusion

## Slide 14: Supply Voltage Control on DRAM
Supply Voltage
Adjust the supply voltage to every chip on the same module
DRAM Module

## Slide 15: Custom Testing Platform
SoftMC [Hassan+, HPCA’17]: FPGA testing platform to
1) Adjust supply voltage to DRAM modules
2) Schedule DRAM commands to DRAM modules
  Existing systems: DRAM commands not exposed to users
Voltage
controller
DRAM
module
FPGA
https://github.com/CMU-SAFARI/DRAM-Voltage-Study

## Slide 16: Tested DRAM Modules
124 DDR3L (low-voltage) DRAM chips
  31 SO-DIMMs
  1.35V (DDR3 uses 1.5V)
  Density: 4Gb per chip
  Three major vendors/manufacturers
  Manufacturing dates: 2014-2016
Iteratively read every bit in each 4Gb chip under a wide range of supply voltage levels: 1.35V to 1.0V (-26%)

## Slide 17: Outline
Executive Summary
Motivation
DRAM Background
Characterization of DRAM
  Experimental methodology
  Impact of voltage on reliability and latency
Voltron: DRAM Energy Reduction Mechanism
Conclusion

## Slide 18: Reliability Worsens with Lower Voltage
Nominal Voltage
Min. voltage (Vmin) without errors
Reducing voltage below Vmin causes an increasing number of errors
Errors induced by reduced-voltage operation

## Slide 19: Source of Errors
Chart: Supply Voltage (V)
| 1.35 | 1.2 | 1.1 | 1.0 | 0.9
Activate | 8.6089 | 8.9382 | 10.0798 | 12.0854 | 16.1766
Precharge | 7.389 | 8.496 | 9.916 | 12.711 | 19.572
Detailed circuit simulations (SPICE) of a DRAM cell array to model the behavior of DRAM operations
Circuit model
Nominal Voltage
https://github.com/CMU-SAFARI/DRAM-Voltage-Study
Reliable low-voltage operation requires higher latency

## Slide 20: DIMMs Operating at Higher Latency
Measured minimum latency that does not cause errors in DRAM modules
Lower bound of latency as our latency adjustment granularity is 2.5ns
Measured Minimum Activate Latency (ns)
8
10
12
14
100% of modules
40% of modules
DRAM requires longer latency to access data without errors at lower voltage
Distribution of latency in the total population

## Slide 21: Spatial Locality of Errors
A module under 1.175V (12% voltage reduction)
Errors concentrate in certain regions

## Slide 22: Other Results in the Paper
Error-Correcting Codes (ECC)
  ECC (SECDED) is not sufficient to mitigate the errors
Effect of temperature
  Higher temperature requires higher latency under some voltage levels
Data retention time
  Lower voltage does not require more frequent refreshes
Effect of stored data pattern on error rate
  Difference is not statistically significant to draw conclusion

## Slide 23: Summary of Key Experimental Observations
Voltage-induced errors increase as voltage reduces further below Vmin
Errors exhibit spatial locality
Increasing the latency of DRAM operations mitigates voltage-induced errors

## Slide 24: Outline
Executive Summary
Motivation
DRAM Background
Characterization of DRAM
  Experimental methodology
  Impact of voltage on reliability and latency
Voltron: DRAM Energy Reduction Mechanism
Conclusion

## Slide 25: DRAM Voltage Adjustment to Reduce Energy
Goal: Exploit the trade-off between voltage and latency to reduce energy consumption
Approach: Reduce DRAM voltage reliably
  Performance loss due to increased latency at lower voltage
Chart: Supply Voltage (V)
| 0.9 | 1.0 | 1.1 | 1.2 | 1.3
Performance | -19.7 | -9 | -4.5 | -2.1 | -0.5
DRAM Power Savings | 33.1 | 23.5 | 16.6 | 9.9 | 3.3
High Power Savings
Bad Performance
Low Power Savings
Good Performance

## Slide 26: Voltron Overview
How do we predict performance loss due to increased latency under low DRAM voltage?
Voltron
User specifies the performance loss target
Select the minimum DRAM voltage without violating the target

## Slide 27: Linear Model to Predict Performance
Voltron
User specifies the performance loss target
Select the minimum DRAM voltage without violating the target
Linear regression model
Application’s characteristics
[1.3V, 1.25V, …]
DRAM Voltage
[-1%, -3%, …]
Predicted performance loss
Min.
Voltage
Target
Final Voltage

## Slide 28: Linear Model to Predict Performance
Application’s characteristics for the model:
  Memory intensity: Frequency of last-level cache misses
  Memory stall time: Amount of time memory requests stall commit inside CPU
Handling multiple applications:
  Predict a performance loss for each application
  Select the minimum voltage that satisfies the performance target for all applications

## Slide 29: Comparison to Prior Work
Prior work: Dynamically scale frequency and voltage of the entire DRAM based on bandwidth demand [David+, ICAC’11]
  Problem: Lowering voltage on the peripheral circuitry decreases channel frequency (memory data throughput)
Voltron: Reduce voltage to only DRAM array without changing the voltage to peripheral circuitry
Peripheral Circuitry
DRAM Array
Control Logic
I/O
Bank
Off-chip channel
Low frequency
Peripheral Circuitry
DRAM Array
Control Logic
I/O
Bank
Off-chip channel
High frequency
Low Voltage
Low Voltage
Prior Work
Voltron

## Slide 30: Exploiting Spatial Locality of Errors
Key idea: Increase the latency only for DRAM banks that observe errors under low voltage
  Benefit: Higher performance
Peripheral Circuitry
DRAM Array
Control Logic
I/O
Bank 0
Off-chip channel
Bank 1
Bank 2
High latency
Low latency

## Slide 31: Outline
Executive Summary
Motivation
DRAM Background
Characterization of DRAM
  Experimental methodology
  Impact of voltage on reliability and latency
Voltron: DRAM Energy Reduction Mechanism
  Evaluation
Conclusion

## Slide 32: Voltron Evaluation Methodology
Cycle-level simulator: Ramulator [CAL’15]
  McPAT and DRAMPower for energy measurement
4-core system with DDR3L memory
Benchmarks: SPEC2006, YCSB
Comparison to prior work: MemDVFS [David+, ICAC’11]
  Dynamic DRAM frequency and voltage scaling
  Scaling based on the memory bandwidth consumption
https://github.com/CMU-SAFARI/ramulator

## Slide 33: Energy Savings with Bounded Performance
Chart: Memory Intensity
| Low | High
MemDVFS | 1.4 | 0.4
Voltron | 3.2 | 7
Chart: Memory Intensity
| Low | High
MemDVFS | -2.7 | -2.1
Voltron | -1.6 | -1.8
Performance Target
[David+, ICAC’11]
More savings for high bandwidth applications
Meets performance target
1. Voltron improves energy for both low and high intensity workloads
2. Voltron satisfies the performance loss target via a regression model
7.3%
3.2%
-1.6%
-1.8%

## Slide 34: Outline
Executive Summary
Motivation
DRAM Background
Characterization of DRAM
  Experimental methodology
  Impact of voltage on reliability and latency
Voltron: DRAM Energy Reduction Mechanism
Conclusion

## Slide 35: Conclusion
DRAM (memory) power is significant in today’s systems
  Existing low-voltage DRAM reduces voltage conservatively
Goal: Understand and exploit the reliability and latency behavior of real DRAM chips under aggressive reduced-voltage operation
Key experimental observations:
  Errors occur and increase with lower voltage
  Errors exhibit spatial locality
  Higher operation latency mitigates voltage-induced errors
Voltron: A new DRAM energy reduction mechanism
  Reduce DRAM voltage without introducing errors
  Use a regression model to select voltage that does not degrade performance beyond a chosen target  7.3% system energy reduction

## Slide 36
Understanding Reduced-Voltage Operation in Modern DRAM Devices
Kevin Chang†
A. Giray Yaglikci†, Saugata Ghose†, Aditya Agrawal*, Niladrish Chatterjee*, Abhijith Kashyap†, Donghyuk Lee*, Mike O’Connor*, Hasan Hassan‡, Onur Mutlu†‡
Experimental Characterization, Analysis, and Mechanisms
†
*
‡

## Slide 37: BACKUP

## Slide 38: Errors Rates Across Modules

## Slide 39: Error Density

## Slide 40: Temperature Impact

## Slide 41: Impact on Retention Time

## Slide 42: Derivation of More Precise Latency
Circuit-level SPICE simulation
DRAM circuit model validates our experimental results and provides more precise latency
Potential latency range

## Slide 43: Performance Loss Correlation
Observation: Application’s performance loss due to higher latency has a strong linear relationship with its memory intensity
Voltage = 1.2V (-13%)
DRAM Latency +5%
Voltage = 1.1V (-23%)
DRAM Latency +13%
MPKI = Last-level cache Misses Per Thousand Instruction
Memory Intensity (MPKI)
Memory Intensity (MPKI)
Performance Degradation (%)

## Slide 44: Performance-Aware Voltage Adjustment
Build a performance (linear-regression) model to predict performance loss based on the selected voltage
𝜽s are trained through 151 application samples
Use the model to select a minimum voltage that satisfies a performance loss target specified by the user
Latency due to voltage adjustment
The running application’s characteristics
Notes: Given this observation, we build a performance model to predict perf…
With this model, there are different ways to make a decision on how to select a voltage.
For example, if the user specifies a 5% loss target for Voltron, Voltron would iteratively go through different voltage levels and select the minimum that it predict would not incur a performance loss greater than the target
Our policy is to select the minimum voltage that does not exceed a performance loss target specified by the user.

## Slide 45: Linear Model Accuracy
R2 = 0.75 / 0.9 for low and high intensity workloads
RMSE = 2.8 / 2.5 for low and high intensity workloads

## Slide 46: Dynamic Voltron

## Slide 47: Effect of Exploiting Error Locality

## Slide 48: Energy Breakdown

## Slide 49: Heterogeneous Workloads

## Slide 50: Performance Target Sweep

## Slide 51: Sensitivity to Profile Interval Length