## Slide 1
The Efficacy of Error Mitigation Techniques for DRAM Retention Failures
Samira Khan*$, Donghyuk Lee*, Yoongu Kim*, Alaa R. Alameldeen$, Chris Wilkerson$, and Onur Mutlu*
*Carnegie Mellon University $Intel Labs
DRAM Scaling Problem
Vision: Online Profiling
Manufacturing Time Testing
PASS
FAIL
PASS
FAIL
Not fully tested during
manufacture-time
Ship modules
with possible failures
1
2
Detect and mitigate
failures online
3
Detect and mitigate errors runtime
  After the system has become operational
Reduces cost of testing, increases yield, enables scaling
We analyze the efficacy of system-level techniques
  Using experimental data from real DIMMs
Efficacy of System-level Detection and Mitigation
Write some pattern
in the module
1
Wait until
refresh interval
2
Read
and verify
3
Only a few rounds can discover most of the failures
Even after hundreds of rounds, a small number of new cells keep failing
Testing alone cannot detect
all possible failures
1
Testing
Adding a safety-margin on the refresh interval
Chart: Time
| 1.0 | 2.0 | 3.0 | 4.0 | 5.0 | 6.0 | 7.0 | 8.0 | 9.0 | 10.0
Retention Time | 110 | 110 | 32 | 32 | 32 | 110 | 110 | 110 | 110 | 110
Column1 | 200 | 200 | 200 | 200 | 200 | 200 | 200 | 40 | 200 | 200
Refresh Interval
2X Guardband
4X Guardband
2
Even a large guardband (5X) cannot detect 5-15% of the intermittently failing cells
Guardbanding
There are few cells with large differences in retention times
Most of the cells exhibit closeby retention times
ECC
Additional information to detect error and correct data
SECDED code reduces error rate by 100 times
Combination of techniques
reduces error rate by 107 times
A combination of mitigation techniques is much more effective
3
Error Correcting Code
Towards an Online Profiling System
Key Observations so far:
1. Testing alone cannot detect all possible failures
2. Combination of ECC and other mitigation techniques is much more effective
- But degrades performance
3. Testing can help to reduce the ECC strength
- Even if we start with a higher strength ECC
Initially Protect DRAM
with Strong ECC
1
Periodically Test
Parts of DRAM
2
Mitigate errors and
reduce ECC
3
Run tests periodically after a short interval at smaller regions of memory
Test
ECC
ECC
DRAM is critical for performance
Demand for high capacity
Scaling enabled higher capacity
Scaling of DRAM results in failures
Intermittent failures are hard to detect
FAIL
PASS
Longer manufacture-time tests, Lower yield, Higher cost
Manufacturing Time Testing
DRAM Intermittent Failures
Leakage
Capacitor
Switch
Refreshed
Every 64 ms
0
1
0
0
0
1
Data Pattern Sensitivity
0
0
0
0
0
2
Variable Retention Time
1
Chart: Time
| 1.0 | 2.0 | 3.0 | 4.0 | 5.0 | 6.0 | 7.0 | 8.0 | 9.0
Retention Time | 512 | 512 | 32 | 32 | 32 | 32 | 512 | 512 | 512