## Slide 1: Improving the Reliability of Chip-Off Forensic Analysis of NAND Flash Memory Devices
Aya Fukami, Saugata Ghose, Yixin Luo, Yu Cai, Onur Mutlu

## Slide 2: Brief Summary of the Paper
Our Goal:
  Identify error sources in NAND flash memory during chip-off
  Quantify errors in NAND flash memory introduced in chip-off
  Identify a mitigation process to reduce errors introduced during chip-off analysis
Our findings:
  Long storage time of devices increases errors in NAND flash memory
  Heat in chip-off increases uncorrectable errors
  Read-retry mechanism can reduce errors introduced during chip-off

## Slide 3: Talk Outline
Background
  Basic operation of NAND flash memory
Testing Methodology and Experimental Results
  Retention error
  Errors introduced by heat
How to Improve Reliability of Chip-off Analysis
  Read-retry operation

## Slide 4: Talk Outline
Background
  Basic operation of NAND flash memory
Testing Methodology and Experimental Results
  Retention error
  Errors introduced by heat
How to Improve Reliability of Chip-off Analysis
  Read-retry operation

## Slide 5: MLC NAND Flash Memory Cell Operation
Current[A]
Voltage[V]
Amount of charge = Threshold voltage of the cell = Stored data value
Stored data: 11
Threshold voltage
Substrate
Drain
Source
Control Gate
Floating
Gate
Oxide
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
01
00
10

## Slide 6: MLC NAND Cell Vth Distribution
11
01
00
10
Threshold Voltage
Number of cells
Read voltage
Threshold voltages need to be between each read voltage

## Slide 7: Retention Error on MLC NAND Flash Cell
11
01
00
10
Threshold Voltage
Number of cells
Charge leakage over time causes threshold voltage shifts
Data error in result is called retention error
–
–
–
–
–
–
–
–
–
Substrate
Drain
Source
Control Gate
Floating
Gate
Oxide
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–
Error!
Error!
Error!
Read voltage

## Slide 8: NAND Flash Cell Degradation
Repeated programming and erasing (P/E cycle) accelerates charge leakage
–
–
–
–
–
–
–
–
–
00
Threshold Voltage
Number of cells
Error!
–
–
–
Erasing
Programming
10
Oxide
Degraded Cell
–
–
–
–
–
–
–
–
–
–
–
–
–
–
–

## Slide 9: NAND Flash Error Sources During Chip-off
Heat guns or electrical rework machines
  De-solder NAND flash memory chips with heat
Required temperature and duration:
250 °C (482 °F), ~2 minutes
High temperature accelerates charge leakage

## Slide 10: Error Correction Codes (ECC)
Flash memory controllers store ECC codewords to correct errors in data
Typical correction capability for recent chip: 40 bits correction capability per 1KB
Errors exceeding ECC correction capability: uncorrectable errors

## Slide 11: Talk Outline
Background
  Basic operation of NAND flash memory
Testing Methodology and Experimental Results
  Retention error
  Errors introduced by heat
How to Improve Reliability of Chip-off Analysis
  Read-retry operation

## Slide 12: Testing Environment
Test chips: New 2y-nm NAND flash memory chips from two different vendors (hereafter called Chip A and Chip B)
Controller: Altera DE0 FPGA

## Slide 13: Testing Methodology: Retention Error Evaluation
Repeated programming/erasing cycles (P/E cycles)
  10, 300, 1000, 2500, and 4000 cycles
Raw bit error rate (RBER) measurement at multiple retention age (=wait time after programming)
  Day 0 and 1, Week 1, 2, 3 and 4

## Slide 14: Experimental Result: Retention Error: Chip A
ECC Error Correction Capability
Chart: P/E Cycle Count
| 10 | 300 | 1000 | 2500 | 4000
Day 0 | 1.0981e-05 | 1.3468e-05 | 3.4254e-05 | 0.00019635 | 0.00034071
Day 1 | 1.1802e-05 | 2.0157e-05 | 5.9332e-05 | 0.0002399 | 0.00049667
Week 1 | 1.8821e-05 | 8.5416e-05 | 0.00039419 | 0.0015734 | 0.0043598
Week 4 | 2.3529e-05 | 0.00010944 | 0.00059884 | 0.0024946 | 0.0065143
10-2
10-3
10-4
10-5
RBER grows as P/E cycle count and retention age increase
12×
18×

## Slide 15: Experimental Result: Retention Error: Chip B
ECC Error Correction Capability
Chart: P/E Cycle Count
| 10 | 300 | 1000 | 2500 | 4000
Day 0 | 3.4716e-05 | 5.5152e-05 | 6.945e-05 | 0.00014624 | 0.00024937
Day 1 | 3.8704e-05 | 6.2273e-05 | 8.4731e-05 | 0.00019569 | 0.00034697
Week 1 | 5.6226e-05 | 9.9976e-05 | 0.00017549 | 0.0005339 | 0.0012398
Week 4 | 6.7009e-05 | 0.00013629 | 0.00028106 | 0.0008268 | 0.001817
10-2
10-3
10-4
10-5
RBER grows as P/E cycle count and retention age increase
3×
4×

## Slide 16: Testing Methodology: Thermal Effect Evaluation
Baking target chips at 250 °C for 2 mins at different retention age (simulating chip-off procedures)
  1 Week
  4 Weeks
Raw bit error rate (RBER) measurement after baking

## Slide 17: Experimental Result: Errors Introduced by Heat (Chip A)
ECC Error Correction
Capability
Chart: P/E Cycle Count
| 10 | 300 | 1000 | 2500 | 4000
Week 1, Before Baking | 1.8821e-05 | 8.5416e-05 | 0.00039419 | 0.0015734 | 0.0043598
Week 4, Before Baking | 2.3529e-05 | 0.00010944 | 0.00059884 | 0.0024946 | 0.0065143
Week 1, After Baking | 0.0011704 | 0.0028207 | 0.015408 | 0.062463 | 0.17429
Week 4, After Baking | 0.00069595 | 0.0056325 | 0.028023 | 0.10148 | 0.15207
100
10-1
10-2
10-3
10-4
10-5
33×
51×
Heat introduces errors more than ECC can correct

## Slide 18: Experimental Result: Errors Introduced by Heat (Chip B)
Chart: P/E Cycle Count
| 10 | 300 | 1000 | 2500 | 4000
Week 1, Before Baking | 5.6226e-05 | 9.9976e-05 | 0.00017549 | 0.0005339 | 0.0012398
Week 4, Before Baking | 6.7009e-05 | 0.00013629 | 0.00028106 | 0.0008268 | 0.001817
Week 1, After Baking | 0.0015959 | 0.0050722 | 0.013054 | 0.024942 | 0.03485
Week 4, After Baking | 0.0014239 | 0.00502 | 0.015163 | 0.04409 | 0.0747
100
10-1
10-2
10-3
10-4
10-5
37×
51x
ECC Error Correction Capability
Heat introduces errors more than ECC can correct

## Slide 19: Experimental Result: Uncorrectable Errors after Baking
Retention Period before Baking | Chip A | Chip B
1 Week | 29.1% | 78.1%
4 Weeks | 84.2% | 83.6%
Fraction of pages that contains uncorrectable errors (P/E cycle=300)
Heat introduces uncorrectable errors
even when the chip has been only lightly used

## Slide 20: Talk Outline
Background
  Basic operation of NAND flash memory
Testing Methodology and Experimental Results
  Retention error
  Errors introduced by heat
How to Improve Reliability of Chip-off Analysis
  Read-retry operation

## Slide 21: Read-Retry Mechanism
11
Threshold Voltage
Number of cells
01 → 11
Default read voltage
Shifted read voltage
Shifted read voltage
01 → 11
Read-retry mechanism shifts the read voltage
to reduce errors caused by threshold voltage shifts
01

## Slide 22: Testing Methodology: Read-Retry Evaluation
Read-Retry command found on chip B
  Implemented as a vendor specific command
Read operation with read-retry
  Evaluation of 2 modes (mode A and B)

## Slide 23: Experimental Result: Error Reduction with Read-Retry
Chart: P/E Cycle Count
| 10 | 300 | 1000 | 2500 | 4000
Default Read | 0.0014239 | 0.00502 | 0.015163 | 0.04409 | 0.0747
Read-Retry Mode A | 0.00013072 | 0.00037249 | 0.001728 | 0.0088076 | 0.019988
Read-Retry Mode B | 0.00029353 | 0.00036881 | 0.00081906 | 0.0049416 | 0.012104
10-1
10-2
10-3
10-4
ECC Error Correction Capability
-88.6%
-94.6%
Read-retry can reduce errors introduced
by thermal-based chip-off procedure

## Slide 24: Uncorrectable Error Reduction by Read-Retry
Read Mode | P/E Cycle Count | 
 | 300 | 1000
Default | 83.6% | 99.7%
Read-Retry A | 0% | 12.1%
Read-Retry B | 0% | 0%
Read-retry can reduce errors introduced
by thermal-based chip-off procedure
Fraction of pages that contains uncorrectable errors (Chip B, after baking)

## Slide 25: Conclusions and Recommendations
Wait time increases errors
  Conduct data extraction at the earliest possible time after receiving a device
Heat introduces uncorrectable errors
  Keep the temperature as low as possible
Read-retry can reduce errors
  Use read-retry after chip-off when available

## Slide 26: Improving the Reliability of Chip-Off Forensic Analysis of NAND Flash Memory Devices
Aya Fukami, Saugata Ghose, Yixin Luo, Yu Cai, Onur Mutlu

## Slide 27: Additional Slides

## Slide 28: NAND Flash Memory Organization

## Slide 29: Retention Error over P/E Cycles
Reproduced from Cai.et.al. “Error Patterns in MLC NAND Flash Memory: Measurement, Characterization, and Analysis” (2012)

## Slide 31
Chart: 1000 P/E Cycles
| 0 | 1 | 7 | 14 | 21 | 28
Default Read | 6.945e-05 | 8.4731e-05 | 0.00017549 | 0.0002056 | 0.00026357 | 0.00028106
Read-Retry Mode A | 0.0026232 | 0.0022481 | 0.0012293 | 0.0010543 | 0.00096672 | 0.00089802
Read-Retry Mode B | 0.0059115 | 0.005273 | 0.0033208 | 0.0028322 | 0.0025012 | 0.0024038
Chart: 2500 P/E Cycles
| 0 | 1 | 7 | 14 | 21 | 28
Default Read | 0.00014624 | 0.00019569 | 0.0005339 | 0.00069014 | 0.00094107 | 0.0008268
Read-Retry Mode A | 0.0056195 | 0.0044357 | 0.0016843 | 0.0014374 | 0.0011667 | 0.0011412
Read-Retry Mode B | 0.013243 | 0.010806 | 0.0039558 | 0.0036176 | 0.0029331 | 0.002677
Chart: 4000 P/E Cycles
| 0 | 1 | 7 | 14 | 21 | 28
Default Read | 0.00024937 | 0.00034697 | 0.0012398 | 0.0014647 | 0.0017348 | 0.001817
Read-Retry Mode A | 0.0081441 | 0.0062538 | 0.0015357 | 0.0014832 | 0.0013382 | 0.0011945
Read-Retry Mode B | 0.021083 | 0.0163 | 0.0035886 | 0.0037698 | 0.0029742 | 0.0027454
Chart: 10 P/E Cycles
| 0 | 1 | 7 | 14 | 21 | 28
Default Read | 3.4716e-05 | 3.8704e-05 | 5.6226e-05 | 6.2874e-05 | 6.8266e-05 | 6.7009e-05
Read-Retry Mode 1 | 0.0010397 | 0.00099005 | 0.0007191 | 0.00064696 | 0.00071147 | 0.00062459
Read-Retry Mode 2 | 0.0028892 | 0.0026628 | 0.0020491 | 0.0018944 | 0.00207 | 0.0015036